## Slide 1
Update on measurements with Si detectors irradiated to 3e17
50 um LGAD (CNM)
New:
1 Mohm bias resistor in Q-TCT amp (Ortec)  possible to measure at higher bias current
Improved cooling  T = - 30 C

## Slide 2
3e16, 650 V
1e17, 1100 V
3e17, 1100 V
Average waveforms

## Slide 3
3e16,
650 V
1e17,
1100 V
3e17
1100 V

## Slide 4
LGAD (50 um): Qmean (V)= ~ 3 x QMPV_spaghetti (V)
Q ~ (dq/dx∙D)∙(1/D)∙L,
L = v∙τ, charge collection distance
v increases with E (until saturation)
At high Ф, saturation at higher V
Magic formula (300 um spaghetti Ф > 1e15):
QMPV = k∙Фb∙V ,
k = 26.4 el/V, b = -0.683
Ф in 1e15 n/cm2, V in volts
 More charge than in spaghetti because of higher E-field and/or charge multiplication

## Slide 5
Edge-TCT with pad detectors– try to measure effective thickness
LGAD – pad detector
difficult to focus on pad detector
 signal from guard ring
~ 50 um active
Double junction
 large signal near top electrode  multiplication
DAC = 57
DAC = 57

## Slide 6
DAC = 57

## Slide 7
1e17
Ponovitve – veliko višji tok?
DAC = 30

## Slide 8
600 um LGAD, 600 V
300 um špageti (1100 V)
Strange charge collection profiles if no good focus???

## Slide 10
LGAD 1e17
Bias = 1100 V
Same detector, ~ 10 days at RT kater
Multiplication?
Breakdown?
~3000 el
~3000 el
Lazarus++

## Slide 11
Calculation:
j = ni ∙E∙(µe+µh)
Eg = 1.12 eV,
me = 1.08 m0
mh = 0.6 m0
Mobility temp scaling:
µ(T) = µ(T0) (T/T0)2.2
Phi = 3e16
µe+µh = 1200 cm2/Vs
(TCT ~ 600)
Phi = 1e17
µe+µh = 800 cm2/Vs
(TCT ~ 400)
Phi = 3e17
µe+µh = 180 cm2/Vs
j vs T at 1 V forward bias

## Slide 12
Mobility
Method from M. Mikuž et al.: mobility estimated from velocity profiles in forward bias
Assumptions: 1) electric field in forward bias: E = V/D, (V bias voltage, D detector thickness)
2) saturation velocity vsat = 190 um/ns does not change with fluence,
3) fit with: v = µ0∙E/(1+µ0∙E/ vsat)
Preliminary!
Good agreement with previous measurements!
Table from M. Mikuž et al.:
Value at 3e17 uncertain  should be interpreted as upper limit
zero field mobility decreases with fluence!
velocity increases linearly with field up to high E