## Slide 1
Dva članka:
  moblitiy vs fluence za nevtrone in protone iz E-TCT meritev (velocity profile) s strip detektorji v forward biasu
   M. Mikuž, TREDI, Paris 2016
  2) CCE meritrve z LGADi do 3e17 in ocene za trapping za visoke fluence
   I. Mandić, TREDI, Vienna 2020

## Slide 2
Mobility:
M. Mikuž, TREDI 2016
dodati še točko za 3e17 za nevtrone
imamo tudi 2e15 za nevtrone do 300 V

## Slide 3
Dashed lines: Q = )
trapping time τ chosen to approximately
match measured data (no minimization …)
 trapping times much longer than
extrapolated from measurements at
low fluences:
1/τext = ẞ∙Ф, ẞ = 5e-16 cm2/ns
CCE in trapping
Forward bias
Fluence (1e16 n/cm2) | τ measured (ns) | τ extrapolated (ns)
2.5 | 0.25 | 0.080
5.7 | 0.18 | 0.035
10 | 0.13 | 0.020
30 | 0.06 | 0.007

## Slide 4
Trapping time
Compare with:
M. Mikuž, TREDI2016:
same approximation as used here, charge measured with reverse biased 300 um spaghetti detectors at 1000 V from G. Kramberger et al., 2013 JINST 8 P08004
 good agreement with measurements with
75 um LGAD
 much larger than extrapolated
with ẞ = 5e-16 cm2/ns