## Slide 1
Development of the monolithic "MALTA" CMOS sensor for the ATLAS ITK outer pixel layer
TWEPP 2018, Antwerp, Belgium, 21.09.2018
B. Hitia, L. Argemib, I. Asensi Tortajadac, I. Berdalovicc, I. Caicedo Sierrad, R. Cardellac, F. Dachsc, V. Daoc, N. Egidos Plajac, T. Hemperekd, H. Krügerd, T. Kugathasanc, C. A. Marin Tobonc, K. Moustakasd, M. Münkerc,d, H. Perneggerc, F. Piroc, P. Riedlerc, P. Rymaszewskid, C. Riegelc, E. J. Schioppac, A. Sharmac,e, W. Snoeysc, C. Solans Sanchezc, T. Wangd, N. Wermesd
a
b
c
d
e

## Slide 2: ATLAS Phase II ITk upgrade
HL-LHC Pixel detector upgrade (2024-2026): 5 pixel layers, inclined layout
Option for the outermost Layer 4: Depleted Monolithic CMOS sensors
Requirements for Pixel Layer 4:
  Radiation tolerance (without safety factors):
    NIEL 1e15 neq/cm2
    TID 60 Mrad
  Hit rate 100 – 200 MHz/cm2
  Timing resolution 25 ns
ATLAS ITk Pixel TDR

## Slide 3: CMOS sensors: Large vs. Small collection electrode
Large collection electrode
Larger capacitance: C ≈ 300 – 400 fF
Higher analog power, sensitive to crosstalk
Uniform, strong drift field, high radiation tolerance and detection efficiency
Smaller capacitance: C ≈ 3 fF  low power
Less sensitive to crosstalk
Longer drift paths
Full depletion can be achieved by modifying the process  radiation tolerance increases
Small collection electrode
M. Garcia-Sciveres and N. Wermes, arXiv:1705.10150

## Slide 4: TowerJazz process: Small collection electrode
Standard process
no full depletion on pixel edges
partially charge collection by diffusion, not radiation tolerant
Modified process
additional low doped n-layer
full depletion, maintains low capacitance, better radiation tolerance, faster charge collection
25 μm
W. Snoeys et al.
DOI 10.1016/j.nima.2017.07.046
TowerJazz 180 nm CMOS imaging process, 4 nested wells, 25 μm p epitaxial layer
Typical bias voltages: -20 V (substrate), -6 V (deep PWELL)

## Slide 5: TowerJazz 180 nm development line
TJ Investigator (2015)
> 250 different pixel flavors
Analog output after CSA
TJ MonoPix (2018)
20 x 10 mm2 half size
Column drain readout
TJ MALTA (2018)
20 x 22 mm2 full size
Asynchronous matrix readout
ALPIDE chip for ALICE ITS upgrade
https://doi.org/10.1016/j.nima.2016.05.016
radiation hardness,
timing, hit rate
x 100
Design team (CERN)
W. Snoeys, T. Kugathasan, C. Marin Tobon, I. Berdalović, R. Cardella, N. Egidos Plaja
Common analog front end design in MALTA and MonoPix
Digital readout designed by University of Bonn
T. Wang et al 2018 JINST 13 C03039

## Slide 6: Charge sensitive front end
Operating principle derived from ALPIDE front end
< 5 fF sensor capacitance  excursion at input of tens of mV
  Voltage amplifier can take the place of a standard CSA
  Optimization for minimal power consumption and fast timing response
Power 0.9 μW, threshold ≈ 200 e-, ENC ≈ 12 e-, gain 0.4 mV/ e-
D. Kim et al. DOI 10.1088/1748-0221/11/02/C02042
M1 acts as a source follower to avoid loading the input
M2 is a cascode transistor to increase the gain on the output node and eliminate the Miller effect for the input node.
The analog output node is stabilized at low frequencies by active feedback on the transistor M3
Efficient current usage for the input (the same branch current powers the source follower and the amplification stage)
MALTA: optional clipping of the analog pulse is implemented
1
2
1 – amplification
2 – discrimination

## Slide 7: TJ MALTA
Analog
Digital
36.4 μm
spacing 3.5 – 4 μm
Novel asynchronous readout, no clock distribution over pixel matrix  reduced power
Low threshold spread, no in-pixel threshold tuning
Analog power ≈ 1 μW per pixel (75 mW/cm2)
Digital power (Layer 4) ≈ 10 mW/cm2
Time-walk based charge information
22 mm
20 mm
512 x 512 pixels, 8 flavors
36.4 μm
MALTA Pixel
Notes: large collecting electrode (LF Monopix) has a power consumption of approx. 200 (ana) + 200 (dig) mW/cm2

## Slide 8: Asynchronous column-drain architecture (MALTA)
Front end discriminator outputs are transmitted asynchronously over high speed bus to chip periphery
2 independent buses serve alternating 2 x 8 pixel groups (one bus for the red groups and another for the blue groups)
  Significantly reduced number of lines per pixel
  Important to minimize probability for data collisions
  Adjustable pulse length 0.5 – 2 ns
22 bits per bus: pixel pattern (16b) + reference (1b) + group address (5b)  22b
I. Berdalovic et al 2018 JINST 13 C01023

## Slide 9: MALTA end of column logic
Asynchronous signals are merged onto a common bus in the periphery
  Adjustment for propagation delay in the parallel data bus
  Column address, time stamp bits added
Arbitration logic (Hit merger) to process simultaneous signals
  One of the signals is delayed to avoid data collisions
  Keeping track of the number of delays, additional delay bits
40 bit output word
Asynchronous hit signals transmitted from the chip via LVDS up to 5 Gbps

## Slide 10: MALTA charge measurement
Charge measurement from time difference between bunch crossing time and leading edge of hit signal
Simulation: Time walk of 25 ns corresponds to 400 e-
Expected time walk 25 ns at 400 e-
charge (ke-)
delay (ns)

## Slide 11: MALTA status
First submission – chips received Jan 2018
  Pixel readout and pixel pulsing functional
  Slow control not fully functional – masking only on double column level, no individual pixels
  Hit merger in the periphery disabled due to too high noise activity  can cause data collisions
Second submission (MLVLC) – chips received Jul 2018
  Modifications aimed at improving ohmic connections in slow control and powering with minimal number of masks
  Chip behavior remained similar to first submission
Future submissions: Mini MALTA – submitted Aug 2018 (MPW)
  Smaller 64 x 16 pixel chip with additional functional blocks
  Slow control redesigned to achieve correct masking, pixel tuning
  Additional synchronization circuit in the periphery to compensate pixel delays at the end of column
Asynchronous readout and slow control with custom readout firmware using Xilinx Virtex-7 VC707 FPGA kit

## Slide 12: TESTING

## Slide 13: TJ Investigator results summary
Analog output from the front end
Good sensor and front end performance after 1e15 neq/cm2 neutron irradiation*:
90Sr measurements:
  < 20 % drop in signal MPV: 18.9 mV  15.9 mV
  Charge collection time 19.0 ns ± 2.8 ns
Test beam (SPS 180 GeV/c pions, FEI4 beam telescope, 9 μm pos. resolution):
  Uniform 98.5 % efficiency within 25 μm pixel (smaller than MALTA)
H. Pernegger et al 2017 JINST 12 P06008
*All neutron irradiations made
at Ljubljana TRIGA reactor
150 e- /mV
threshold 50 e-

## Slide 14: Threshold scan – TJ MonoPix
Tail due to random telegraph signal noise
Threshold distribution
271 e- ± 31 e-
K. Moustakas et al, arXiv:1809.03434
ENC 11 e-
Measurement of S-curves by injecting test charge into front end
Before irradiation: thr. 271 e- ± 31 e-, ENC 11 e-
After irradiation: thr. 470 e- ± 50 e-, ENC 20 e- (1.5e15 neq/cm2 neutrons, 1 Mrad TID)
Increase in noise may require in-pixel threshold adjustment
Threshold measurement in MALTA not trivial (no masking), extracted distribution compatible with MonoPix
Front end almost identical in TJ Monopix and MALTA – expect same threshold values
TJ MonoPix
before irradiation

## Slide 15: MALTA test beam
SPS test beam, 180 GeV/c pions, Mimosa beam telescope, 5 μm position resolution
Before irradiation: avg. efficiency 96 % (less in corners)
Efficiency loss due to noise
  Merger circuit and pixel masking not available
  Track hit and a noise hit arrive simultaneously (within 1 ns)
  Data is misinterpreted as a hit coming from another pixel  not matched with telescope track
Efficiency map (unirrad.)
https://doi.org/10.1016/j.nima.2014.05.033.
In-pixel efficiency (unirrad.)
avg. efficiency 96 %
Optimal HV bias configuration SUB -15 V, PWELL -6 V
IMON2 = 1.36 V
TODO: threshold value

## Slide 16: MALTA test beam irradiated
1e15 neq/cm2 neutron irradiated sample
Critical efficiency loss in pixel corners after irradiation
  Noise increases in irradiated samples  higher threshold required to suppress noisy pixels (no masking/merging !)
  Threshold too high to detect hits on pixel edges (charge sharing)
  Efficiency correlated with deep PWELL distribution – inspired modifications discussed with the foundry (next slide)
Inefficiency in the centers due to a high noise level (efficiency in centers increases at a higher threshold !)
PosX (μm)
PosY (μm)
avg eff. 74 %
High threshold
inefficiency for low signals
Low threshold
inefficiency due to noise
Deep PWELL distribution
IMON2 = 1.38 V

## Slide 17: Fixes discussed/planned with the foundry
Additional deep p-type implant
Requires additional mask, but can use 'known' process step
Creating a gap in the deep n-type implant
Mask change, no additional mask required
Both changes target modifying electrical field on pixel edges to improve charge collection – simulation

## Slide 18: 2D Device simulation
original MALTA/MonoPix
time (s)
current (A)
Simulation by M. Münker, Bonn & CERN
modified
original
modified
original
Both Additional PWELL Implant and Gap in n- Implant expected to significantly improve charge collection
pix. size 40 μm
unirrad.
1e15 neq/cm2
pix. size 30 μm
40 μm
40 μm
Large penalty for increased pixel pitch
Signal collection from pixel corner

## Slide 19: Summary
After encouraging results on first prototypes, designed two monolithic CMOS sensors for the ATLAS ITk upgrade with a small low capacitance collection electrode layout for low analog power consumption
  Monopix: more conservative synchronous column-drain readout
  Malta: novel asynchronous readout without clock distribution over the matrix to minimize power consumption (< 100 mW/cm2)
Degraded detection efficiency, especially in the pixel corners, due to:
  Higher threshold spread than expected from simulations,
  further degraded after irradiation
  Non-gaussian tail in the noise due to random telegraph noise
  The increased pixel pitch, effect confirmed also by TCAD simulations
  Slow control issue on Malta
  (unability to correctly mask and therefore large number of noise hits and constraint to stay at higher threshold)
  Degraded efficiency correlated with deep PWELL layout
This initiated:
  Development of threshold tuning and front end study (not yet completed)
  Collaboration with the foundry and extensive TCAD simulations to improve charge collection by mask or process modification and submission of a MiniMalta test chip in an MPW including a first version of these fixes in August
Test beam | Average eff. | Eff. in corners
unirradiated | 96 % | 90 %
1e15 neq/cm2 | 75 % | < 40 %
Malta efficiency

## Slide 20: Acknowledgements
We thank TowerJazz for their constructive collaboration

## Slide 21: BACKUP

## Slide 22: MALTA chip
power pads
allow chip-to-chip bonding

## Slide 23: TJ MonoPix
1 x 2 cm2 chip (224 x 224 pixels)
Column drain readout
4 sectors with different pixel flavors
  Improved low power column bus readout
  Standard PMOS input reset
  Adaptive input reset (leakage compensation)
  Frontside HV biased, AC coupled pixels
Pixel size 36 μm x 40 μm
Low threshold dispersion, no in-pixel tuning
ToT charge information
Analog power < 1 μW per pixel (65 mW/cm2)
Digital power (Layer 4) ≈ 100 mW/cm2
T. Wang et al 2018 JINST 13 C03039

## Slide 24: Front end optimization (simulation)
sensing node
amplifier output
discriminator output
pulse duration clipping (MALTA)
dead time
time walk
I. Berdalovic et al 2018 JINST 13 C01023

## Slide 25: Adaptive PMOS reset
Circuit for reseting input in some pixel flavors
At high frequencies (hit)
fast input Reset
adjustable
At low frequencies (leakage)
Low frequency feedback
Compensate for IL
Stability has to be guaranteed

## Slide 26: MALTA propagation delay
analog output of one of the pulsed pixels
Reference signals (asynchronous 2 ns pulse for each hit)
Measured delay between first two pulses 12.2 ns
Propagation delay of asynchronous signals through double column bus up to 8 ns

## Slide 27: MALTA 55Fe spectrum
Analog output from the front end
Separation between Kα and Kβ lines before and after irradiation
Front end configuration not the same  signal size not directly comparable

## Slide 28: MALTA threshold
Measurement of S-curves by electronically injecting charge in the front end
  Charge calibration calculated from injection capacitance
Without fully functional slow control difficult to measure correctly
  Fit error function and make a χ2 cut on fit quality
  Analyzing only S-curves which passed the cut
Samples (unirradiated):
  W4R7 – Jan 2018
  W6R6 – Jul 2018
Thresholds
  371 e- ± 43 e- (W4R7)
    550 e- ± 53 e- (W6R6)
    10 % threshold spread
    calibration verification necessary, f.e. 55Fe
  After irradiation noise level increases substantially
high pulse amplitude
W6R6
W4R7
entries

## Slide 29: MALTA threshold scan
Chip status
  Merger is disabled, therefore high traffic in the output will resolve in incorrect reconstruction
  Each slow control command is preceded by lowering VDD to 1.2V and followed by raising VDD to 1.8V
  Cannot mask top half pixels
  Fixed threshold settings (IMON2=1.3 V)
Algorithm
  Mask all the chip
  Unmask selected column
  Enable pulsing on selected pixel up to row 20
  Change pulse size
  Enable read-out, pulse, disable read-out
    Repeat 500 times
  Readout all hits in buffer
  Only selected pixel + row 251 and 511 should respond

## Slide 30: MALTA test beam unirradiated
In-pixel efficiency map (2 x 2 pixels), unirradiated, low threshold
Sample W4R7 (Jan 2018)
Lower (90 %) efficiency in corners
Overall efficiency > 96 %
Sample W6R6 (Jul 2018)
Lower (93 %) efficiency in centers
  Threshold is higher
  Efficiency loss in center when signal is low
  Shared hits on edges – higher probability to detect at least one of two hits
Overall efficiency > 96 %
Discrepancy between samples likely due to difference in threshold level, since process is unchanged
Optimal HV bias configuration SUB -15 V, PWELL -6 V

## Slide 31: MALTA hit timing
Time of arrival for hits matched with a track
  Peaked distribution as expected
  In-time efficiency ignored for now
Time of arrival for hits not matched with a track
  For noise expecting uniform distribution
  Indicates false hit reconstruction due to data collisions (merger circuit is disabled !)
Detection efficiency can be increased by improvement of electronical sector
Masking individual pixels  remove noisy pixels
Per pixel threshold tuning ?
Merger circuit
unirradiated sample

## Slide 32: MALTA test beam irradiated
1e15 neq/cm2 neutron irradiated sample (first submission)
(moderately)
high threshold
avg eff. 72 %
IMON2 = 1.30 V
low threshold
avg eff. 74 %
IMON2 = 1.38 V
2 x 2 pixels
PosX (μm)
PosY (μm)
PosX (μm)
PosY (μm)
At a higher threshold:
Efficiency in corners reduces (expected)
Efficiency in centers increases: Lower noise level  smaller probability for data collisions due to disabled merger

## Slide 33: MALTA test beam irradiated
Cluster size 1
Cluster size 2
Cluster size > 2
1e15 neq/cm2 neutron irradiated sample (first submission)
In-pixel cluster size

## Slide 34: Device simulation
First TCAD Simulation of charge collection after irradiation
2D simulation for simplicity, 3D in progress
  Simulation in the plane on the diagonal between two pixels ("worst case")
  Charge injected in the corner between four pixels
Simulation by M. Münker, Bonn

## Slide 35: Device simulation model
Physics ( material = "Silicon" ) {
Traps (
( Acceptor Level fromCondBand Conc=@<fluence*1.613> @ EnergyMid=0.42 eXsection=1E-15 hXsection=1E-14 )
( Acceptor Level fromCondBand Conc=@<fluence*0.9> @ EnergyMid=0.46 eXsection=5E-15 hXsection=5E-14 )
( Donor Level fromValBand Conc= @<fluence*0.9> @ EnergyMid=0.36 eXsection=3.23E-13 hXsection=3.23E-14 )
# fromCondBand: relative to the conduction band
# Conc: N_0 of radiation level (different energetic distributions of traps, e.g. exponential)
# EnergyMid: defines the energy level with respect to the defined reference level (in this case relative to the conduction band)
# The factors after the fluency are the “introduction rate” -> rate of defect levels produced for a certain dose)
}
Parameters (from: IEEE Trans.Nucl.Sci. 63 (2016) 2716-2723, DOI: 10.1109/TNS.2016.2599560)