## Slide 1
Results of TCT and Sr-90 measurements with ATLAS17LS detectors
Igor Mandić, Vladimir Cindro et al.,
Jožef Stefan Institute, Ljubljana, Slovenia
ATLAS Upgrade Week, CERN, November 2018

## Slide 2
Motivation
results of measurements with A17LS mini detectors irradiated with 28 MeV protons at Birmingham
after irradiation with 5e14 n/cm2 protons at Birmingham:
   low collected charge
   large cluster size
See presentation at Itk week in Oxord:
https://indico.cern.ch/event/726191/contributions/3151464/attachments/1722835/2782344/ITkStripSensors_MS3-tests_2018-09-26_v4.pdf
Measurements from Birmingham:

## Slide 3
Results from Santa Cruz (Sean Riedel, Cole Helling et al.)
For proton-irradiated sensors (Birmingham) see a charge deficit for fluences>= 5e14 neq/cm^2
•Gets worse after annealing.
•CYRIC-irradiated sensor after annealing looks ok.
Motivation
results of measurements with A17LS mini detectors irradiated with 28 MeV protons at Birmingham
See presentation at Itk week in Oxord:
https://indico.cern.ch/event/726191/contributions/3151464/attachments/1722835/2782344/ITkStripSensors_MS3-tests_2018-09-26_v4.pdf

## Slide 4
Samples and measurements
Devices irradiated with protons 28 MeV at Birmingham:
ATLAS17LS mini strip detector (W32, mini 8) to 5e14 n/cm2  Edge–TCT and Top-TCT
8 mm x 8 mm diodes
 I-V (1e14 and 5e14)
 charge collection measurements with Sr-90: 1e14 (W30, 1-3), 5e14 and 1e15 (W29, 1-2) and
2e15 (W32,1-3)
ATALS17 LS mini strip detectors irradiated to 5e14 at CYRIC (W12, mini8), and CERN PS (W36, mini2) TCT

## Slide 5
I-V measurements (Vladimir Cindro)
measured with 8 x 8 mm2 diodes irradiated in Birmingham
at 700 V extract value of α after annealing for 80 minutes at 60 °C
theoretically expect: 4e-17 A/cm
 package was warm when received
 detectors annealed for few days at RT during transport
Target fluence 1e14 n/cm2:
Diode 1: α = 2.8e-17 A/cm
Diode 2: α = 2.1e-17 A/cm
Target fluence 5e14 n/cm2:
Diode 3: α = 6.5e-17 A/cm
indicates fluence smaller than target
or too much annealing
or current measurement error
 fluences ~ OK, may be max. 50% different than target fluences
Points to larger than target fluence but:
I-V curve not very nice
current from depleted volume
could be overestimated

## Slide 6: Single channel 90Sr setup
ORTEC-142 charge sensitive amplifier + 25 ns shaper
Calibrated with a 300 µm thick Si pad detector
Measured at T = -30°C up to ~ 550 V
 measurements of collected charge with diodes
detector
ORTEC 142 charge sensitive amplifier + custom made shaper (25 ns)
+ digital oscilloscope
ampl.
90Sr
PMT
cooling jig
DUT

## Slide 7
Results from mini-strips from: V. Cindro, Hiroshima 2017
https://doi.org/10.1016/j.nima.2018.10.007
Diodes (A17LS) irradiated at Birmingham
Collected charge, Sr-90, diodes
diode irradiated to 1e14 n/cm2 in Birmingham looks OK
diodes irradiated to 5e14, 1e15, 2e15 n/cm2 in Birmingham:
  much lower charge than with minis irradiated with neutrons or protons at CYRIC
  (expect somewhat less charge with diodes but the difference should be smaller)
  collected charge drops after annealing for 80 minutes at 60°C
 consistent with charge collection measurements with mini strip detectors (Birmingham, Santa Cruz, Toronto)

## Slide 8
Edge TCT
Velocity profile:
Induced current at t ~ 0 (immediately after the laser pulse)  proportional to carrier velocity at laser spot location
 if E not too large, I proportional to E ( Ew ~ constant, see: G. Kramberger, et al.,IEEE Trans. Nucl. Sci. NS-57 (2010) 2294.)

## Slide 9
Edge TCT
velocity profiles after irradiation at Birmingham very different than after irradiation at CYRIC or CERN-PS or neutrons
 high carrier velocity (electric field) near back plane (y = 300 µm)
 looks like n-type bulk
CYRIC, CERN-PS and neutron profiles look as expected
 differences between protons (CYRIC and CERN-PS) and neutrons can be explained by the oxygen in the substrate material
profile after neutron irradiation measured with ATLAS12EC-R0 mini detectors  same substrate as A17LS
depth
det. surface

## Slide 10
Edge TCT
Measurements with ATLAS12A sensors form 2015
(See e.g.: I. Mandic, ITK strip sensor meeting 20. October 2015, https://indico.cern.ch/event/448475/)
Compare:
neutrons
Karlsruhe protons (23 MeV)  closest to Birmingham protons (28 MeV)
24 GeV protons,
PSI pions (300 MeV)
500 V
Effect of Karlsruhe protons most similar to
the effect of neutrons in ATLAS12A sensors

## Slide 11
One strip connected to amplifier
and to HV via Bias-T
Surrounding strips and
bias ring connected to HV supply
Metal: connected to same potential (HV supply)!
 weighting field as when connected to multi-channel readout chip!
Top TCT
Narrow laser beam directed to the top surface
More detail about Top-TCT in:
Mandić et al., “TCT measurements of
irradiated strip detectors with a focused
laser beam”, 2013 JINST 8 P04016
or slides of RD50 meeting in Bari in2012
https://indico.cern.ch/event/175330/contributions/
283763/attachments/
225128/315042/Mandic_Bari_2012.pdf

## Slide 12
much larger contribution to the charge on signal strip from carriers drifting far away in detector irradiated in Birmingham
  large charge sharing and therefore large cluster size
  consistent with large field and large charge collection near the back plane seen by Edge -TCT
Top TCT
metal on signal strip
connected to the amplifier
Laser beam perpendicular to
detector surface
move the beam in steps across
detector surface perpendicular
to the strips
points show charge collected on signal strip
when laser beam at this point

## Slide 13
Conclusions:
unusual behavior of A17LS detectors irradiated with protons in Birmingham  different than after irradiation with neutrons or
protons at CYRIC or CERN-PS
effect of Birmingham protons in this irradiation different than effect of 23 MeV protons in Karlsruhe on ATLAS12A detectors
(measured in2015)
Edge-TCT shows large back side electric field  looks like “type inversion” to n-type bulk
Top-TCT indicates more charge sharing after Birmingham irradiation  consistent with high field at the back seen by E-TCT
Low collected charge measured with Sr-90 with diodes for irradiated in Birmingham to 5e14, 1e15 and 2e15,
drop of charge collection after short term annealing
 consistent with charge collection measurements with mini detectors made by other groups
type inversion in p-type material and drop of collected charge after short (beneficial) annealing seen only in epitaxial silicon
irradiated at CERN-PS (e.g. P. Dias de Almeida, RD50 workshop https://indico.cern.ch/event/663851/contributions/2788203/ ,
or Khomenkov et al., 2008 IEEE Nuclear Science Symposium Conference Record, 10.1109/NSSMIC.2008.4774876 )
effects seen in this irradiation not understood  why this behaviour only with Birmingham protons and not with other proton sources?
Outlook:
repeat irradiation of ATLAS17LS minis and diodes in Birmingham

## Slide 14
3) Gibljivost nosilcev v visoko obsevanem siliciju

## Slide 15
I-V pri 1 V forward
Calculation:
Eg = 1.12 eV
Phi = 3e16
mu_e+mu_h = 1500
Phi = 1e17
mu_e+mu_h = 900
Phi = 3e17
mu_e + mu_h = 300
Gibljivosti večje kot merjeno s TCT

## Slide 16
Mobility
Method from M. Mikuž et al.: mobility estimated from velocity profiles in forward bias
Assumptions: 1) electric field in forward bias: E = V/D, (V bias voltage, D detector thickness)
2) saturation velocity vsat = 190 um/ns does not change with fluence,
3) fit with: v = µ0∙E/(1+µ0∙E/ vsat)
Preliminary!
Good agreement with previous measurements!
Table from M. Mikuž et al.:
Value at 3e17 uncertain  should be interpreted as upper limit
zero field mobility decreases with fluence!
velocity increases linearly with field up to high E

## Slide 17
Forward 30 V
Reverse 1000 V
Revers 300 V
1e15, 24 GeV protons
E-TCT, ponovitev meritvev za detector, ki se je čudno obnašal
Merili praktikanti letos poleti

## Slide 19
Obsevanje NurFET radfetov v IRRAD v CERNu, oktober 2018
Turški radfeti, 120 nm debelina oksida, test za morebitno uporabo za radiation monitor v Itk
Obsevanje gama v reaktorju
Kalibracija s Cz137
Veliko prenizka dozna hitrost
 Pričakuješ ~20 cGy/s??
Krambi:

## Slide 20
24 mm
32 mm
40 mm
20 mm
Top view
Side view
~10 mm
~18 mm
Temp senor

## Slide 21
žarek

## Slide 22
Temperaturna odvisnost pred obsevanjem
25 uA boljše kot 200 uA
nižji tok bolj ugoden, ker rabimo nižjo napetost

## Slide 23
Dozna hitrost cca. 1 Mrad/h (3e13 p/cm2/h)
Saturacija po cca 6 h  to je 6 Mrad (60 kGy) ali 2e14 p/cm2 je 1.2e14 n_eq/cm2
Radfeti v žarku
Radfeti 7 mm izven
žarka
Žarek se je malo odpeljal

## Slide 24
Zoom in the structure at 350 minutes. Fading can be seen.
Radfet in the central position
Radfet 7 mm off-centre
Vidimo da output pada čeprav se najbrž še vedno nekoliko obseva.
Uporabno dinamično območje je verjetno dosti pod 2e14 p/cm2

## Slide 25
Annealilng:
manj obsevani radfeti so pod saturacijo čitalca (~ 25 V)
bolj obsevani so še vedno nad 25 V
Radfete še vedno beremo, nov plot čez nekaj tednov

## Slide 26
Zaključek:
NurFET zazna sevanje
Problem je fading po hadronski dozi
Najbrž ni slabši kot REM radfeti
 potrebnih bo še kar nekaj testov
 kalibracijo z nabitimi hadroni pri nižji dozni hitrosti