## Slide 1: Peel tests - neutron irradiated flexes
samples – coverlayer on copper
Irradiated to 2 1015 ncm-2, ≈ 20 kGy
Peel tester KJ-1065B Computer type Peeling strength tester
Sample width 50mm
Peel speed 10 mm/min
Force averaged over 30 mmm length

## Slide 2
Test reports

## Slide 4: Test results
TID – 600 kGy
Neutron irradiated
2 1015 ncm-2