## Slide 1
Testbeam results from BCM' campaign at SPS in Oct2021
F9 meeting, 11.02.2022
Bojan Hiti, F9, Jožef Stefan Institute (JSI)

## Slide 2: Overview
pCVD diamond sensor + custom front end (Calypso)
  Pad detector (mm2), 4 channels per FE chip
Test beam with MALTA telescope at SPS in Aug, Oct, Nov 2021
Oct 2021 SPS run log:
  200000 – 200021: 2.5x2.5 mm2 single crystal (SC) diamond sensor diamond thickness 500 um
  200022 – 200039: 10x10 mm2 pCVD diamond (4 pads area 1:4:2:8)
  200040 – 200047: 5x5 mm2 pCVD (board failed)
  200048 – 200070: 3d diamond (positive HV)
  200071 – 200086: 4 mm2 silicon
  200087 – 200094: 3d diamond (negative HV)
  200095 – 200113: another 5x5 mm2 pCVD (rotated 25°)
  200114 – 200119: 3d diamond

## Slide 3
DUT
MALTA telescope
DRS4

## Slide 4: Trigger and readout
Trigger:
MALTA ROI
Delayed PMT
AND
DRS4
ch4
(trigger on waveform)
trig
out
MALTA
1.8 V, 200 ns
Needs external 50 Ohm termination on telescope side!
DUT readout:
  Sensors wire bonded to CALYPSO Front End
  Analog and digital signals read out by DRS 4 (3 ch. per run)
    4 GS/s, 700 MHz bandwidth
  In Nov 2021 three DRS4 daisy chained for more channels (9 ch. per run)
  CALYPSO specifications:
  Optimized for Cdet 2–5 pF
  tpeak < 1.5 ns, tsettling < 15 ns
  digital LVDS output, analog preamp output for testing
AMP
thr
discr.
LVDS+
LVDS-
analog out
Calypso front end
DUT IN
Trigger enable window (120 ns)

## Slide 5: Signal sampling
Signal = integral of waveform over sampling window
  Algorithm will be improved
  Today's results are very preliminary!
In the past Out-of-time signals in 3 % of events
  Efficiency not above 96 %
  Caused by trigger jitter from the telescope
  Remedied by Timing cuts on telescope signals (next slide)
    now spectacular tracking
signal (mV)
t (1 bin = 0.25 ns)

## Slide 6: Results – Silicon (200081)
Analog output
efficiency
pulse height
track distribution
Timing cut here

## Slide 7: Results – Silicon (200081)
Digital output

## Slide 8: Results – SC diamond (200006)
Analog output
efficiency
pulse height
track distribution

## Slide 9: Results – pCVD diamond (200043)
Analog output
efficiency
pulse height
track distribution

## Slide 10: Results – pCVD diamond (200043)
Digital output
efficiency
pulse height
track distribution

## Slide 11: Results – 3d diamond – square (200050)
Analog output
efficiency
pulse height
track distribution

## Slide 12: Results – 3d diamond – hex (200069)
Analog output
efficiency
pulse height
track distribution

## Slide 13: Results – pCVD diamond digital signals
Same analysis, but with digital signals (after on-chip discriminator)
  Limited number of events analyzed up to now
Threshold setting "medium" (no noise figure available)
Three pads with different sizes  capacitance affects efficiency