## Slide 1
Irradiations of ATLAS Itk strips QA samples with protons at CERN PS (IRRAD)

## Slide 2
IRRA irradiation 2021
IRRAD irradiation setup 2022
irradiated cold
during shipment ~ 7 days at RT
0 min intentional annealing probably roughly equivalent
to annealing of ~ 80 min at 60 C

## Slide 3
Uniformity of irradiation
This QA irradiation (plot made by Vitaliy):
J. Keller, J Kroll,
https://indico.cern.ch/event/694901/contributions/2849730/
subcontributions/247249/attachments/1588666/2513066/Keller18-01-24.pdf
PS beam profile
x: FWHM = 8.7 mm
 scanning possible
y: FWHM = 12.1 mm
position of the device in the beam matters
any misalignment can cause significant effects, especially if there is no scanning

## Slide 4
Current
sample VPA8186- W1304 nominal Фeq = 1e14 n/cm
 at this fluence Vfd ~ 200 V
 measured with MD8 diode at 20C after annealing 80 min at 60 C
 simple diode structure (but guard rings not contacted)
measured current much higher than expected
I-V
C-V
Vfd ~ 200 V
Mini detectors
current higher than after neutron irradiation to same fluence
 higher than I=V∙α∙Фeq (indicated by arrows in the graph)
Protons 1.6e15
1.6e15
1e15
5e14
1e14
Are actual fluences higher than nominal?

## Slide 5
PS irradiation results with A17 presented at strip sensor meeting 23. Nov. 2018 https://indico.cern.ch/event/776393/
IRRAD irradiation (2021,2022): 1.6e15: current ~ 35 uA @ 500 V
 consistent with 2018 measurements
with: Фeq = 1.5e15 n/cm2 , α = 4e-17 Acm, T = -20°C, fully depleted mini sensor, area 8x8 mm2: I = 21 µA
 current larger than calculated
 after neutron irradiation to 1.6e15 current ~ 20 uA @ 500 V
A17, PS irradiation, 2018
U. Soldevila
Current

## Slide 6
Charge collection
PS protons 1.6e15: consistent with 2021
Much smaller than after 1.6e15 neutrons

## Slide 7
These are 26 MeV and 70 MeV protons
Compare with previous IRRAD irradiations
K. Hara et al., NIMA 983 (2020) 164422
https://doi.org/10.1016/j.nima.2020.164422
results from 2018: PS protons at Ф > 1e15 similar as neutrons
irradiation of QA samples with PS protons (2021)
 lower than expected but not very far from results with A17
 measured ~ 6 ± 1 ke…. , expected ~ 8 ± 1 ke
in these measurements CCE after neutron irradiation lower than after protons
  but no IRRAD data
K. Hara et al., NIMA 831 (2016) 181-188
https://doi.org/10.1016/j.nima.2016.04.035
IRRAD 22
IRRAD 21
QA Ljub

## Slide 8
Annealing
Charge drops with annealing
 note: 0 min means ~ 7 days at RT
Current drops with annealing

## Slide 9
E-TCT test with QA minis irradiated with 24 GeV protons in IRRAD
because of dimensions and cutting of the sample E-TCT was measured with laser along the strip
  different weighting field than in “standard” configuration with laser perpendicular to the strip direction
  charge generated only under one strip therefore weighting field “realistic”  as when charged particle crosses
Standard E-TCT doesn’t work well
because of too wide edge
Laser
Scan under the strip form top to back side

## Slide 10
PS protons, 1.6e15
900 V
700 V
500 V
300 V
100 V
900 V
700 V
500 V
300 V
100 V
Neutrons 1.6e15
VPA38186-W1297
Edge TCT
different charge collection profiles for neutrons and protons at same Фeq
  rapid drop of profile height with bias voltage
   for neutrons profile under strip gets narrower but height doesn’t drop so rapidly as in the case of protons
(narrower total profile width in proton sample (it is less than 300 um) because of polishing  see next slide)
PS protons, 1e15
900 V
700 V
500 V
300 V
100 V
VPA38186-W1299

## Slide 11
Polishing quality
Neutron sample 1.6e15 (VPX37412-W704)
PS protons (1.6e15) VPA38186-W1297
Edge damaged by polishing, no or small E-TCT signal from this part

## Slide 12
E - TCT profiles
PS protons
1.6e15
Bias = 500V
Sensor depth
strip
VPA38186-W1297
Neutrons
1.6e15
Bias = 500V
Sensor depth
strip
VPX37412-W704
PS protons
Neutrons
large differences between charge collection profiles for proton and neutron irradiation
significant contribution of charge from the back of detector after proton irradiation
 field at back (low weighting potential)  reduces field at front (high weighting potential)  smaller charge collection

## Slide 13
E - TCT profiles
Sensor depth
strip
VPA38186-W1297
PS protons
1.6e15
Bias = 500V
Neutrons
1.6e15
Bias = 500V
Sensor depth
strip
VPX37412-W704
PS protons
1e15
Bias = 500 V

## Slide 14
Older results with PS protons
A. Affolder, P. Allport, G. Casse NIMA623 (2010)177–179, https://doi.org/10.1016/j.nima.2010.02.187
FZ p-type, MCZ p-type
 not much difference can be seen between pions, MeV protons, GeV protons and neutrons above 1e15 n/cm2
FZ material
MCZ
(no PS protons)