## Slide 1: Sample preparation for HGTD Long Term Stability test
Bojan Hiti
Jožef Stefan Institute
15 March 2024

## Slide 2: Board 1
Shape of Tesa conductive tape strips
B1 Sample 1 –V1R5-49 0e14
B1 Sample 2 –V1R5-46 15e14
irradiated samples annealed 80 min @ 60 °C

## Slide 3: Sensor bonding
All 15 x 15 pads connected together and connected to readout via 1 kOhm resistor
Guard ring connected to ground via separate 1 kOhm resistor
“Leaf” pads – can be made floating by tearing their wire bond

## Slide 4: Readout & Guard Ring connection detail
Using both Bump Bond and Probe Needle pads on some pixels