## Slide 1: ATLAS High Granularity Timing Detector and Production Activities at F9
Bojan Hiti
Jožef Stefan Institute
Seminar, February 2024

## Slide 2: Outline
Part 1: ATLAS-HGTD at HL-LHC
  HL-LHC and motivation for ATLAS-HGTD
  HGTD detector components
    LGAD Sensors
    Readout chip
    Integration into experiment
Part 2: ATLAS-HGTD production activities at JSI F9
  Sensor Process Quality Control
  Sensor Irradiation Tests
  Production of Flex Tail circuits

## Slide 3
Part 1: ATLAS-HGTD at HL-LHC

## Slide 4: High Luminosity LHC (HL-LHC)
schedule updated January 2022
ATLAS experiment pileup:
LHC run 3: <μ> = 40
HL-LHC: <μ> = 200
Collisions within
30–60 mm
175–260 ps

## Slide 5: ATLAS phase II upgrade
[slide from T. Affolder, Lepton Photon 2021]

## Slide 6: ATLAS High Granularity Timing Detector
Pile-up a big experimental challenge at HL-LHC
  At <μ> = 200 most probable pile-up density 1.44 vertices/mm  vertex spacing 0.6 mm
  New tracker ATLAS ITk alone not sufficient for vertex separation in forward direction
600 μm
z0 resolution with ITk only
σ = 50 ps
ITk
HGTD
ATLAS High Granularity Timing Detector (HGTD)
  Track time information, resolution 50 ps
  In addition luminosity measurement by particle counting (target 1 % precision)

## Slide 7: ATLAS HGTD basic information
total thickness 75 mm
active region
12 cm < r < 64 cm
Rapidity coverage | 2.4 < ¦η¦< 4.0
Position in z | ± 3.5 m
Number of channels | 3.6 M
Pad size | 1.3 mm × 1.3 mm
Operating temperature | –30 °C (CO2)
Time resolution (beginning) | 30 ps
Time resolution (End-Of-Life) | 50 ps
location between barrel and endcap calorimeters
Two double sided instrumented layers
(= 4 sensor layers)

## Slide 8: HGTD Radiation Environment
Radiation damage in HGTD after 4000 fb-1 up to 8.3e15 neq cm-2, 7.5 MGy (including safety factors)
HGTD designed for End-of-Life (EOL) fluence 2.5 × 1015 neq cm-2, TID 2 MGy  detector replacements planned
Segmentation in three concentric rings:
    Inner ring (r ≤ 230 mm) replaced every 1000 fb-1
    Middle ring (r < 470 mm) replaced at 2000 fb-1
    Outer ring (r < 640 mm) will not be replaced
1
2
3

## Slide 9: HGTD Modules
Module = two single-chip Hybrids (sensor + readout chip) connected to the same flex PCB (Module Flex)
  Total dimension 2 cm × 4 cm
  15 × 30 channels (15 × 15 per hybrid), 1.3 mm × 1.3 mm channel size
Total of 8032 modules
  Rows of hybrids connected via Flex Tails to the Peripheral Electronics Boards (PEB) @ 660 < r < 920 mm
Module overlap optimized on each ring, ensure 2–3 hits per track
modules
PEB

## Slide 10: HGTD Sensors: Low Gain Avalanche Detector (LGAD)
Hit time resolution ≤ 70 ps per layer is required - beyond standard HEP devices
Low Gain Avalanche Detector (LGAD) – new silicon sensor technology pioneered by CNM Barcelona and CERN-RD50
  n-on-p silicon sensor with additional p+ Gain Layer
  Charge multiplication by impact ionization – improved Signal-to-Noise
  Operation in linear regime with typical gain factor 10–20
Active sensor thickness 50 μm, physical thickness of silicon 300 μm
+
Landau .. non uniform charge deposition by MIP (limit 25 ps in 50 μm thick sensors)
Elec .. due to readout electronics (25 ps/70 ps – start of HL-LHC/4000 fb-1) Clock .. due to LHC clock jitter (15 ps)
[G. Pellegrini, G. Kramberger et al.: Technology developments and first measurements of Low Gain Avalanche Detectors (LGAD) for high energy physics applications, NIM A, 2014]

## Slide 11: Why gain?
To minimize noise jitter fast signals with high Signal-to-Noise ratio are required
To minimize Landau fluctuation contribution need thin detectors
but less signal, need Gain
LGAD requirements for HGTD: 4 fC collected charge after 2.5e15
50 ps LGAD time resolution
1 fc = 6250 e-

## Slide 12: LGAD radiation effects
LGAD internal gain vital for a good time resolution
Impact ionization increases exponentially with electric field in gain layer  LGAD performance critically depends on voltage drop in Gain Layer
Displacement damage by irradiation reduces effective doping concentration in p-type silicon
  Acceptor removal: electrically active Boron gets deactivated by formation of the BiOi defect  NB, Vgl reduces
  Larger bias voltage needed to sustain the same E-field/Gain  but physical limits
Defect engineering to improve radiation hardness
  Carbon coimplantation to screen Boron in the lattice  slower removal
Vgl .. gain layer depletion voltage
depends on Gain Layer doping NB
Nb .. effective acceptor concentration
w .. gain layer thickness (1–2 μm)
d .. active device thickness (50 μm)
10s of Volts
From sensor overdepletion
100s of Volts

## Slide 13: LGAD Single Event Burnout (SEB)
Single Event Burnout – Catastrophic failure in highly irradiated LGAD devices
  Caused in particle beam by rare events with massive charge deposition (10s MeV)
  Localized destructive electrical breakdown, “crater”
Threshold at average electric field in LGAD exceeding 11 V/µm (550 V for 50 µm thick devices)
“Natural limit” for LGAD radiation hardness
  Cannot further increase bias voltage to mitigate gain loss due to radiation damage

## Slide 14: LGAD radiation hardness
Since 2014 extensive R&D program for development and optimization of LGAD devices for HL-LHC
Evaluated prototypes from 5+ manufacturers
Carbon enriched designs meet HGTD radiation hardness specifications
For HGTD production selected two Chinese designs:
  IHEP-IME (Beijing, China)
  USTC-IME (Hefei, China)
LGAD sensor preproduction started in 2023

## Slide 15: ALTIROC: HGTD readout chip
ASIC produced in 130 nm CMOS process by TSMC (radhard)
Pixel chip with low number of channels optimized for timing
  Small jitter: 25 ps at 10 fC (< 70 ps at 4 fC)
  2 fC minimum discriminator threshold
Time-to-Digital Converters (TDC) for measurements of
  Time of Arrival, w.r.t. LHC clock
  Time over Threshold, for time walk correction using constant fraction discrimination
Development status
  ALTIROC 0 & 1: small prototypes for analog front end tests
  ALTIROC 2: First full size prototype (15 × 15 pixels) with full electronic chain
  ALTIROC 3: Current version, performance up to specifications on testbench and after irradiation
  ALTIROC A: Planned production version, minor fixes to ALTIROC 3 design, planned submission February 2024

## Slide 16: Peripheral Electronics Board (PEB)
Circuit for distribution of services & control to modules, data aggregation and optical links
Located at 660 < r < 920 mm
“The most complex electrical circuit of high energy physics”
  Up to 9 groups with 12 lpGBTs, 52 Bpol12v, support up to 55 front-end modules per PCB
  22 layer PCB, Micro-via size down to 0.1 mm – difficult manufacturing

## Slide 17: HGTD module and detector assembly
Module Production: Hybridization  Flex gluing Metrology  Wire bonding  Module testing
  6 assembly sites – Europe, Morocco, China
10s of Modules grouped into Detector Units – mechanical support and cooling
  24 Detector Units per quarter disk
Flex tails to connect modules with Peripheral Electronic Boards
54-Module Demonstrator being assembled at CERN
  Two out of four Detector Units delivered

## Slide 18: HGTD production timeline
Sensors
ALTIROC
Module Flex
Support Units
Flex Tails
PEB
Hybridization
Modules
Detector Units
HGTD A
HGTD C
Feb 2024
Spring 2027
Fall 2026
prepared for installation

## Slide 19
Part 2: ATLAS-HGTD at F9

## Slide 20: ATLAS HGTD at F9 – 3 activities
1 Process Quality Control
2 Sensor Irradiation Tests
3 Flex tail production
Current HGTD team:
G. Kramberger, B. Hiti, I. Velkovska, J. Debevc, M. Terglav
Past Members:
A. Howard, Ž. Kljun, L. Potočnik

## Slide 21: HGTD Production Sensor & QCTS
> 21.000 good Sensors (≈ 1000 wafers) will be required for HGTD
Produced on 8-inch wafers
  90 % IHEP-IME design, 10 % USTC-IME design
  Each wafer holds 52 Main Sensors (15×15, 2×2 cm)
Dedicated Quality Control Test Structure (QCTS) adjacent to each Main Sensor
  Used for Quality Control throughout production
Current status of HGTD preproduction (5 % of total):
  7 wafers distributed for preliminary testing
  130+ wafers in last stages of processing (UBM deposition)
  5 sites involved in sensor Quality Control testing:
    IHEP (China), USTC (China), CERN, Sao Paulo (Brazil), JSI
main 15 x 15 sensor
QCTS

## Slide 22: F9 HGTD Process Quality Control
Standardized monitoring of sensor properties on each wafer via QCTS
  Check if manufacturing process parameters within specification – PQC
  Probe card (30 needle) used to contact all structures simultaneously
  Automated electrical test performed
Baseline: PQC with unirradiated samples from each wafer
Main test sites are Sao Paulo (also DAQ development) and CERN
JSI is backup site in case of problems
  Jernej Debevc working on setup commissioning
1 x 1 LGAD, 1 x 2 LGAD
- LGAD performance
PIN diode
- Si bulk properties
MOS Capacitor
- SiO2 properties
Van der Pauw structures
- Resistivity measurement
Gate Controlled Diodes
- Surface currents

## Slide 23: F9 HGTD Irradiation Tests
Irradiation Tests (IT) to monitor sensor radiation hardness throughout production
  LGAD radiation hardness very sensitive to manufacturing variations (1 % variation in [B] makes a difference)
  Neutron irradiation at JSI TRIGA reactor and performance characterization at JSI  JSI is the main test site
  Run 1–2 tests on each wafer (total ≈ 1000 tests)
  Must be fast and well understood – new TCT method developed
  Wafer acceptance criteria – will be based on statistics from multiple samples
Goals:
  Check that sensor performance within specifications after EOL fluence of 2.5 × 1015 neq cm-2 (4 fC @ 550 V, 50 ps)
  Also group similar wafers for building modules (in ATLAS two sensors will share same high voltage)
Samples tested in HGTD preproduction:
  5 + 2 wafers (IHEP + USTC)
  Neutron fluences 4e14 – 3.5e15 neq cm-2, annealing 80 min at 60° C
  Some samples irradiated above EOL fluence to ensure they fail IT
IT in scope of ATLAS Qualification Task by Iskra Velkovska, measurements also by student Matic Terglav

## Slide 24: CV: Acceptor removal parameter
  CV: Acceptor removal parameter c in all IHEP-IME and USTC-IME wafers is around 1e-16 cm-2 (slight differences)
  Promising result in terms of acceptor removal  indicates good radiation hardness
USTC-IME
IHEP-IME

## Slide 25: IT – TCT test method
New laser TCT based test method developed for IT
Charge collection measurement with a focused infrared laser
  Top-TCT, room temperature
Test structure 1 × 2 LGAD on QCTS
  Interpad region: LGAD–PIN–LGAD
  No gain in interpad region – PIN diode (= standard silicon pad sensor)
  Measure LGAD performance and calibrate it against PIN
optical window for laser beam
laser beam (FWHM 10 µm)
scan direction
Particulars setup

## Slide 26: TCT-IT concept
Slide taken from P. Skomina, 42nd RD50 Workshop
LGAD1
LGAD2
GAP
both LGADs connected to same readout channel

## Slide 27: TCT-IT method
  Measure collected charge as a function of voltage in LGADs and PIN and determine:
    Gain layer depletion voltage Vgl – onset of observable signal
    Sensor depletion voltage Vfd – end of sharp signal increase
    Gain vs. bias voltage A – ratio of LGAD and PIN collected charge
    Interpad distance – between both LGADs
    Leakage current
  These parameters are used to qualify sensor performance/radiation hardness
  Indirect method – calibration against other methods
LGAD1
LGAD2
PIN
Collected charge (a.u.)
beam direction
scan direction
Vbias = 100 V
charge = signal integral [0, 3 ns]

## Slide 28: TCT-IT Quality of Life improvements
Sample placement: dedicated Al holder with a groove for precise placement
  Precise orientation and known position (simpler & faster measurement preparation)
Fixing screw
+
Rubber washer
groove
scan direction
Sample in focus
Sample out of focus
Data quality test Automated check that sample is in beam focus
degraded charge measurement in PIN
Automated analysis scripts and uploading of results in CERN production database

## Slide 29: TCT-IT Results: Vgl
Vgl as a function of fluence for different wafers
Falling consistently with fluence (acceptor removal)
  Clear separation between fluences – good sensitivity
Results reasonably consistent between wafers
USTC-IME samples do not follow the trend of IHEP-IME
  Data comes from first measurements during method commissioning – learning curve
  More statistics required when samples available
Chart: TCT-IT Vgl vs Fluence
| 0 | 800000000000000 | 1500000000000000 | 1500000000000000 | 2500000000000000 | 2500000000000000
IHEP W1 | 23.2 | 20.3 | 18.3 | 19.4 | 17.8 | 17.7
IHEP W2 | 23.9 | 16.3 | 15.9
IHEP W3 | 23.4 | 16.4 | 16
IHEP W4 | 20.5 | 19.7 | 18.7
USTC W2 | 20.4 | 17
USTC W24 | 19.3 | 17.5

## Slide 30: TCT-IT Results: Gain
LGAD Gain at 100 V (= fixed voltage)
Falling consistently with fluence (due to smaller Vgl)
  Relatively good separation between fluences – sensitivity
More statistics needed for fluences ≥ 2.5e15 to determine measurement uncertainty
More statistics required, especially with USTC-IME
Chart: TCT-IT Gain@100 V vs Fluence
| 0 | 800000000000000 | 1500000000000000 | 1500000000000000 | 2500000000000000 | 2500000000000000
IHEP W1 | 13 | 5.9 | 4.2 | 4.3 | 3.4 | 3.4
IHEP W2 | 20 | 3.1 | 3.2
IHEP W3 | 23 | 3.2 | 2.6
IHEP W4 | 5.8 | 3.7 | 3.8
USTC W2 | 4 | 2.3
USTC W24 | 4.8 | 3
0e14
13 - 20

## Slide 31: IT: systematic effects
Extensive setup validation studies during TCT-IT commissioning to evaluate systematic effects
No nasty systematic effects found
Gain @ 100 V
Vgl (V)
Temperature dependence [-30°C, 20°C]
Sample | T (K) | Vgl (V) | Gain at 100 V
V1R2-21_1.5e15 | 293 | 18.1 / 18.2 | 4.2/4.1
 |  | 18.3 / 18.3 | 4.1/4.2
 |  | 18.4 / 18.4 | 4.2/4.2
Reproducibility (3× same test)
20 °C
-30 °C
LGAD2
LGAD1
gap
Mechanical shifts with temperature

## Slide 32: 90Sr measurements
  TCT-IT not directly measuring MIP charge and time resolution
  Charge Collection and Time Resolution measured with Sr90 and used for TCT-IT calibration
    Sr90 is a pure β emitter – laboratory MIP source
  Setup with two LGADs (time reference and DUT)
    DUT cooled to –30° C
    Trigger on reference LGAD + PMT (“MIP” selection)
    DUT not part of the trigger
  Up to 2 measurements per day, relatively time consuming
    In production will only be used for diagnostics of problematic wafers / occasional calibration

## Slide 33: Sr90 results: charge and time resolution
Chart: Collected charge (-30 °C)
| 120 | 130 | 140 | 150 | 160
W1 0e14 (IHEP) | 9 | 11.5 | 13.7 | 16.5 | 21.5
W1 8e14 (IHEP) | 7 | 7.5 | 8 | 9 | 11 | 14 | 20 | 33
W1 8e14 (JSI) | 4 | 7.8144 | 9.5097 | 13.1122 | 17.992 | 23.6132 | 26.9609
W1 15e14 (IHEP) | 5 | 6 | 7 | 8 | 8 | 9.5 | 11.5 | 17 | 26
W1 15e14 (JSI) | 4 | 4.9341 | 7.1658 | 10.7588 | 16.5509 | 20.3448 | 25.5018
USTC W2 15e14 (JSI) | 5.646 | 6.64 | 8.6802 | 12.1199 | 17.5112 | 23.128
W1 25e14 (IHEP) | 4 | 4.3 | 4.6 | 5 | 6 | 7.5 | 10.5 | 14.5 | 4 | 4 | 4.2 | 4.5 | 4.6 | 4.7 | 4.9 | 5 | 5.5 | 7 | 9 | 12
W1 25e14 (JSI) | 4.0371 | 4.5989 | 5.0714 | 6.2992 | 7.3161 | 8.0514 | 9.1863 | 10.0795 | 10.1658 | 11.4854 | 12.0033 | 12.7017
Chart: Time resolution Wafer 1 (-30 °C)
| 120 | 130 | 140 | 150 | 160
W1 0e14 (IHEP) | 40 | 36.5 | 29.5 | 27.5 | 28
W1 8e14 (IHEP) | 55 | 49 | 46 | 43 | 42 | 37.5 | 38 | 29.5
W1 8e14 (JSI) | 43.3424 | 39.5644 | 36.2442 | 35.7755 | 33.4862
W1 15e14 (IHEP) | 60 | 57 | 56.5 | 49 | 46 | 44 | 43 | 38 | 30
W1 15e14 (JSI) | 43.8178 | 45.7051 | 41.0983 | 40.4189 | 36.9367 | 37.1123 | 35.4447
W1 25e14 (IHEP) | 63 | 58 | 55 | 51 | 47 | 45 | 40 | 38.5 | 56 | 55 | 54 | 55 | 52 | 54 | 54 | 50 | 49 | 44 | 37.5 | 38
W1 25e14 (JSI) | 46.1736 | 43.8178 | 45.3412 | 40.8682 | 40.1852 | 38.4627 | 38.9823 | 37.2562 | 38.4194 | 36.6817
  Results between wafers and manufacturers very similar (do not see the discrepancy from TCT-IT)
  Same sample measured first at JSI, then IHEP  excellent agreement
  HGTD Preproduction: Collected charge and time resolution well within specifications even at EOL fluence
operational regime outside specifications (4 fC, 50 ps, 550 V)

## Slide 34: Sr90 results at extreme fluences (3e15, 3.5e15)
Excellent performance of all wafers up to now. How do we know what IT failure will look like?
 Sample irradiation above EOL fluence: 3e15, 3.5e15 neq/cm2
Chart: Collected charge (-30 °C)
| 475 | 500 | 525 | 550 | 575 | 576 | 601
W2 30e14 | 3.6467 | 3.9223 | 4.6811 | 4.7305 | 5.2366 | 5.147 | 5.393
W2 35e14 | 4.0246 | 4.0151 | 4.7048 | 4.7282 | 5.4945 | 6.4 | 6.9732
W3 30e14 | 4.6334 | 4.8 | 5.1142 | 4.9314 | 4.7792 | 7.2048 | 8.1766
W3 35e14 | 2.6795 | 2.96 | 3.514 | 4.24 | 5.3703 | 5.7795 | 7.393
Collected charge just above 4 fC at 550 V
This indicates rough acceptance criteria in TCT-IT:
  Vgl > 17 V @ 2.5e15 (for IHEP-IME)
  Gain(100 V) > 3 @ 2.5e15 (for IHEP-IME)

## Slide 35: Outlook: Wafer Acceptance/Rejection process
Predefined Acceptance Criteria
Irradiation to 1.5e15 (2.5e15 ? ),
≈ 5 QCTS/wafer
TCT-IT sample 1
?
OK
Not OK
TCT-IT sample 2
?
OK
Not OK
TCT-IT sample 3
?
OK
Not OK
Wafer accepted
PQC sample 1
Sr90
Wafer rejected
Occasional full (irradiated) sensor test on probe station, compare to specs (Maybe)
Predefined Acceptance Criteria
Will constrain parameters (in some yet undefined way*):
Vgl, Gain (100 V), Ileak, Interpad distance, (Sr90 charge)
*Based on statistical distributions of tested samples, for example 2σ

## Slide 36: ATLAS HGTD Flex Tail production
Flex Tails: lightweight multichannel cables connecting HGTD modules with Peripheral Electronic Boards
  Built on Polymide (Kapton) substrate – flexible
  Many stacked on top of each other  small thickness
≈ 10,000 pieces, 79 flavors (lengths)
  5 cm–70 cm, same connector ends, different body length
JSI has experience with flex cable production for ITk strip endcap modules – collaboration with SLO industry (Elgoline)
  Potential for further collaboration in HGTD
Current activity status
  HGTD 54-module Demonstrator being built
  JSI provided 5 prototype flex cables – work OK
  Vendor selection and production orders not yet done

## Slide 37: HGTD Flex Tail MoU
  JSI to provide:
    8.5 % of total Flex Tails
    33.3 % of total Flex Tail testing
    Irradiation tests
  FPGA based test setup copied from Uni Mainz for testing

## Slide 38: Summary
  ATLAS HGTD for HL-LHC is a step forward in particle detector technology
  It will provide:
    Precise particle timing information ≤ 50 ps (!)
    Bonus: Luminosity measurement (1 %)
  LGAD sensors – technology developed in HEP (including JSI) for HL-LHC detectors
  Preproduction currently ongoing, planned completion of HGTD A/C in Fall 2026/Spring 2027
  Production activities at F9
    Process Quality Control – backup site
    Irradiation Test Quality Control – main site, new test method developed
    Flex tail production – cooperation with Slovenian industry