## Slide 1: First-principles screening of mineral candidates for dark matter detection with the PALEOCCENE technique
Vsevolod Ivanov
Virginia Tech NSI & Department of Physics
May 20, 2025

## Slide 2: Outline
Overview of PALEOCCENE & Material Requirements
Role of Color Center Defects
Candidate Minerals & Requirements
Alkali Halide Defects & Formation Mechanisms
Vacancy clusters in LiF
Computational Considerations - Koopman’s Tuning & Electron-Phonon Coupling
Formation mechanisms
Forsterite, Scheelite, Corundum, & Zircon
Which simple defects are optically bright and visible?
Nudged Elastic Band method for energy barriers

## Slide 3: Outline
Overview of PALEOCCENE & Material Requirements
Role of Color Center Defects
Candidate Minerals & Requirements
Alkali Halide Defects & Formation Mechanisms
Vacancy clusters in LiF
Computational Considerations - Koopman’s Tuning & Electron-Phonon Coupling
Formation mechanisms
Forsterite, Scheelite, Corundum, & Zircon
Which simple defects are optically bright and visible?
Nudged Elastic Band method for energy barriers

## Slide 4
Overview
MDvDM | Yokohama | May 2025
Idea: Minerals in the earth’s crust can potentially be detectors with exposures approaching 109 kg-years.
The lowest energy nuclear recoils create atom-scale crystal defects, which may be detected optically as color centers.

## Slide 5
Mineral Requirements
Cosmological backgrounds become negligible with ~5km of rock shielding
High temperatures cause defect annealing! –avoid historically hot or geologically active regions
Samples must be large, high-quality single crystals (not amorphous rock)
Low concentrations of Uranium/Thorium
Synthetic version available for R&D
MDvDM | Yokohama | May 2025

## Slide 6
Mineral Candidate List
Mineral Nat. Abundant Synth. Avail ≥1 km Low U/Th__
Diamond ✓ ✓ ✓ ✓
Olivine ({Mg/Fe}SiO4) ✓ ? ✓ ✓
Zircon (ZrSiO4) ✓ ? ? ✓
Alkali Halide (LiF, NaCl,…) ✓ ✓ ✓ ✓
Quartz (SiO2) ✓ ✓ ✓ ✓
Corundum (Al2O3) ✓ ✓ ? ✓
Apatite ✓ ✓ ? ?
Monazite X ? ? ?
Zirconia (ZrO2) X ✓ X ✓
Scheelite (CaWO4) X ✓ ? ✓
MDvDM | Yokohama | May 2025

## Slide 7
Mineral Candidate List
Mineral Nat. Abundant Synth. Avail ≥1 km Low U/Th__
Diamond ✓ ✓ ✓ ✓
Olivine ({Mg/Fe}SiO4) ✓ ? ✓ ✓
Zircon (ZrSiO4) ✓ ? ? ✓
Alkali Halide (LiF, NaCl,…) ✓ ✓ ✓ ✓
Quartz (SiO2) ✓ ✓ ✓ ✓
Corundum (Al2O3) ✓ ✓ ? ✓
Apatite ✓ ✓ ? ?
Monazite X ? ? ?
Zirconia (ZrO2) X ✓ X ✓
Scheelite (CaWO4) X ✓ ? ✓
MDvDM | Yokohama | May 2025

## Slide 8
Quartz (SiO2)
MDvDM | Yokohama | May 2025
J. Chem. Phys. 14 July 2015; 143 (2): 024505 Materials (Basel). 2021 Dec 13;14(24):7682
Main color center is the E’ defect
Many other optically inactive defects! MD predicts ~500 unidentified defects for each E’ center!
Reason - flexible structure & flat potential surface – also why silica has many structural polymorphs
Zirconia (ZrO2) also has same issue

## Slide 9
Mineral Candidate List
Mineral Nat. Abundant Synth. Avail ≥1 km Low U/Th__
Diamond ✓ ✓ ✓ ✓
Olivine ({Mg/Fe}SiO4) ✓ ? ✓ ✓
Zircon (ZrSiO4) ✓ ? ? ✓
Alkali Halide (LiF, NaCl,…) ✓ ✓ ✓ ✓
Quartz (SiO2) ✓ ✓ ✓ ✓
Corundum (Al2O3) ✓ ✓ ? ✓
Apatite ✓ ✓ ? ?
Monazite X ? ? ?
Zirconia (ZrO2) X ✓ X ✓
Scheelite (CaWO4) X ✓ ? ✓
MDvDM | Yokohama | May 2025

## Slide 10
Diamond
MDvDM | Yokohama | May 2025
ADAQ database:
https://defects.anyterial.se/
Data on 20,000+ defects in diamond is already available!
Part of current efforts to identify color center spin-qubits for QIS
Our contribution: https://www.quantumdefects.com

## Slide 11
Mineral Candidate List
Mineral Nat. Abundant Synth. Avail ≥1 km Low U/Th__
Diamond ✓ ✓ ✓ ✓
Olivine ({Mg/Fe}SiO4) ✓ ? ✓ ✓
Zircon (ZrSiO4) ✓ ? ? ✓
Alkali Halide (LiF, NaCl,…) ✓ ✓ ✓ ✓
Quartz (SiO2) ✓ ✓ ✓ ✓
Corundum (Al2O3) ✓ ✓ ? ✓
Apatite ✓ ✓ ? ?
Monazite X ? ? ?
Zirconia (ZrO2) X ✓ X ✓
Scheelite (CaWO4) X ✓ ? ✓
MDvDM | Yokohama | May 2025
✓

## Slide 12
Mineral Candidate List
Mineral Nat. Abundant Synth. Avail ≥1 km Low U/Th__
Diamond ✓ ✓ ✓ ✓
Olivine ({Mg/Fe}SiO4) ✓ ? ✓ ✓
Zircon (ZrSiO4) ✓ ? ? ✓
Alkali Halide (LiF, NaCl,…) ✓ ✓ ✓ ✓
Quartz (SiO2) ✓ ✓ ✓ ✓
Corundum (Al2O3) ✓ ✓ ? ✓
Apatite ✓ ✓ ? ?
Monazite X ? ? ?
Zirconia (ZrO2) X ✓ X ✓
Scheelite (CaWO4) X ✓ ? ✓
MDvDM | Yokohama | May 2025
✓
→ Use ab initio calculations to determine which mineral is ideal for PALEOCCENE (many simple interstitials/vacancies that are optically bright + visible spectrum)

## Slide 13: Outline
Overview of PALEOCCENE & Material Requirements
Role of Color Center Defects
Candidate Minerals & Requirements
Alkali Halide Defects & Formation Mechanisms
Vacancy clusters in LiF
Computational Considerations - Koopman’s Tuning & Electron-Phonon Coupling
Formation mechanisms
Forsterite, Scheelite, Corundum, & Zircon
Which simple defects are optically bright and visible?
Nudged Elastic Band method for energy barriers

## Slide 14
Irradiated Alkali Halides
Goldstein (1896) – alkali halides bombarded by cathode rays change color!
MDvDM | Yokohama | May 2025

## Slide 15
Abundance of Color Centers!
Journal of Luminescence 100 (2002) 333–343
MDvDM | Yokohama | May 2025

## Slide 16
Simulation Considerations
MDvDM | Yokohama | May 2025
Defect is embedded into a large supercell of 200-500 atoms (256 for LiF)
For each charge/spin state, the ground state structure is relaxed first with DFT, then hybrid functional methods
Hybrid functionals mix DFT with Hartree-Fock simulations, set by two parameters (α – mixing, μ – cutoff range)
Excited states approximated using ∆SCF method (unoccupy/occupy orbitals). Note – this ignores exciton/many-body effects!

## Slide 17
Generalized Koopmans’ Theorem
Generalized Koopmans Theorem:
∆HOMO – position of the highest occupied level relative to the conduction band
∆LUMO – position of the lowest unoccupied level relative to the conduction band
∆IE – vertical ionization energy
gKT: ∆HOMO = ∆LUMO = ∆IE
https://arxiv.org/abs/2412.21060
MDvDM | Yokohama | May 2025

## Slide 18
Generalized Koopmans’ Theorem
Generalized Koopmans Theorem:
∆HOMO – position of the highest occupied level relative to the conduction band
∆LUMO – position of the lowest unoccupied level relative to the conduction band
∆IE – vertical ionization energy
gKT: ∆HOMO = ∆LUMO = ∆IE
https://arxiv.org/abs/2412.21060
MDvDM | Yokohama | May 2025

## Slide 19
Strong el-ph Coupling!
J. Phys. Chem. Solids Vol. 52, No. I. pp. 249-297. 1991
MDvDM | Yokohama | May 2025

## Slide 20
Defect Data
https://arxiv.org/abs/2412.21060
MDvDM | Yokohama | May 2025

## Slide 21
Defect Data
https://arxiv.org/abs/2412.21060
MDvDM | Yokohama | May 2025

## Slide 22
Defect Data
https://arxiv.org/abs/2412.21060
MDvDM | Yokohama | May 2025
These defects are highly delocalized! → Need larger Supercell

## Slide 23
Defect Data
Phys. Rev. B 54, 17508
MDvDM | Yokohama | May 2025

## Slide 24
Electronic Structures
Overall decent match to experimental PL!
What about formation energy? How do we understand PL annealing changes?
https://arxiv.org/abs/2412.21060
F
F2-
F20
F2+
F3+
F30
F3-
MDvDM | Yokohama | May 2025

## Slide 25
Electronic Structures
Overall decent match to experimental PL!
What about formation energy? How do we understand PL annealing changes?
https://arxiv.org/abs/2412.21060
F
F2-
F20
F2+
F3+
F30
F3-
MDvDM | Yokohama | May 2025

## Slide 26
Defect formation dynamics: what happens after irradiation?
After formation, F-centers rapidly recombine into F2 and F3+ defects – rates can be determined by photoluminescence measurements as samples anneal over time.
How can we determine reaction rates from first principles?
MDvDM | Yokohama | May 2025

## Slide 27
Defect formation dynamics: what happens after irradiation?
MDvDM | Yokohama | May 2025
Arrhenius equation – rate given by activation energy:
Need to consider all reaction pathways! Ex: the vacancy concentration over time:
where are the rates for vacancies combining with or an interstitial fluoride ion.
So, we need activation energy!
Find Ea for this reaction using NEB method
Can these be extracted from Laplace transform of PL decay?

## Slide 28
Nudged Elastic Band Method
MDvDM | Yokohama | May 2025
Initial and final configurations are linked by a linear interpolation images. Structure relaxed with images constrained by connecting spring forces:

## Slide 29
Nudged Elastic Band Method
MDvDM | Yokohama | May 2025
Initial and final configurations are linked by a linear interpolation images. Structure relaxed with images constrained by connecting spring forces:

## Slide 30
Nudged Elastic Band Method
MDvDM | Yokohama | May 2025
Initial and final configurations are linked by a linear interpolation images. Structure relaxed with images constrained by connecting spring forces:

## Slide 31
Nudged Elastic Band Method
MDvDM | Yokohama | May 2025
Ea for formation is ~3.5 eV
Ea for recombination is only ~0.5eV
With increasing distance, end state energy will decrease

## Slide 32: Outline
Overview of PALEOCCENE & Material Requirements
Role of Color Center Defects
Candidate Minerals & Requirements
Alkali Halide Defects & Formation Mechanisms
Vacancy clusters in LiF
Computational Considerations - Koopman’s Tuning & Electron-Phonon Coupling
Formation mechanisms
Forsterite, Scheelite, Corundum, & Zircon
Which simple defects are optically bright and visible?
Nudged Elastic Band method for energy barriers

## Slide 33
Screening Materials for MDDM (in progress)
MDvDM | Yokohama | May 2025
Treat materials with HSE06 (reproduces band gap for non-polar materials)
“simple” defects, i.e. neutral vacancies/self-interstitials (clusters & charged in progress)
Ground state energy ∆ ~ ZPL ± 0.2eV (known from defect database). Visible: 3.1-1.8eV. For simplicity ignore el-ph effects.
The ideal material for MDDM will have mostly optically active “simple” defects.

## Slide 34
Corundum (Al2O3)
MDvDM | Yokohama | May 2025
O-vacancy has only 1 transition – outside vis (~250nm)
Al-vacancy has several transitions 1.4-2.3eV (545-890nm) , all relatively bright (0.2-1.4 Debye2)
O-vac
Al-vac

## Slide 35
Corundum (Al2O3)
MDvDM | Yokohama | May 2025
Interstitial Al puts Fermi level in the conduction band (supercell may be too small?)
Interstitial O has two transitions at ~3.1eV, both dark
O-int
Al-int

## Slide 36
Olivine
MDvDM | Yokohama | May 2025
Mixture of MgSiO4 (forsterite) & FeSiO4 (fayalite). Fayalite is magnetic, so focusing on forsterite
O-vac: (4.45eV/280nm), dim (TDM ~0.05 Debye2)
Si-vac: 4 transitions (2.6-3.6eV), two dark, two dim (TDM ~0.1 Debye2)
Mg-vac: 2 transitions (1.7eV/740nm), 1 very bright!
Natural olivine is a mixture of Mg/Fe – will cause broadening, other effects
O-vac
Si-vac
Mg-vac

## Slide 37
Scheelite (CaWO4)
MDvDM | Yokohama | May 2025
Only data for O-vac available:
1 transition (2.55eV/490nm), dim (TDM ~0.1 Debye2)

## Slide 38
Zircon (ZrSiO4)
MDvDM | Yokohama | May 2025
Several defects (Si/Zr are high spin)
O-vac: 1 bright 4eV transition (TDM ~6.5 Debye2)
Si-vac: Several bright transitions 3-3.4eV
Zr-vac: Many transitions 1.4-2.2eV (860-570nm), most moderately bright
O-vac
Si-vac
Zr-vac

## Slide 39
Mineral Candidate Summary
Mineral Abundant Synth. ≥1 km Low U/Th__ Color Centers (400-700nm)
Olivine (MgSiO4) ✓ ? ✓ ✓ 2-3/3*
Zircon (ZrSiO4) ✓ ? ? ✓ 3/3
Corundum (Al2O3) ✓ ✓ ? ✓ 0-1/4
Scheelite (CaWO4) X ✓ ? ✓ 1/1
MDvDM | Yokohama | May 2025
Comments:
HSE energy level ∆ overestimates ZPL – true transitions will be shifted towards red/IR
For Olivine, effect of solid solution MgSiO4/FeSiO4 needs to be understood
Larger defect clusters/charge states need to be checked
Need to compare with absorption/PL spectra – experimental verification needed!

## Slide 40
Thanks for Listening!
This work is supported by NSF GCR Grant OIA-2428507.
https://www.condensedmatters.com/
The group!
Thank you Keegan, Giti, Brenden, & Patrick for LiF measurements!
https://arxiv.org/abs/2503.20732
MDvDM | Yokohama | May 2025
https://arxiv.org/abs/2412.21060