## Slide 1: Measurements with a heavily annealed production QC-TS
Bojan Hiti on behalf of jsi group
HGTD Sensor meeting, 2 march 2026

## Slide 2: Samples
Annealed at 40 °C for 80–120 kmin (2 – 3 months)
  Pilot batch
  B4-10-5, B4-16-5  tested with Sr90
  B4-13-5  todo
These samples have been used for C-V tests by Brigita
Bonded 1x1 LGAD + Guard Ring
  Large noise + breakdowns observed without GR starting at -200 V
    This probably also happens in TCT

## Slide 3: Annealing at different temperatures
Voltage required for G~ 20 vs time
(40oC)
(60oC)
(80oC)
Measured at 20oC and 500 V
Measured at 20oC and 500 V
Gain at 500 V vs time
(40oC)
(60oC)
(80oC)
around an order of magnitude difference in time constants (similar to long term reverse annealing of Neff)
sanity check: GI=20 corresponds to GQ=10 is around ~6 fC
G. Kramberger, HGTD week Feb 2026

## Slide 4: B4-10-5 (“worse performance”)
T = [-31, -30] °C
0.1 µA/fC

## Slide 5: B4-13-5
T = [-29, -28] °C
< 0.1 µA/fC

## Slide 6: B4-16-5 (“better performance”)
T = [-31, -30] °C
< 0.1 µA/fC

## Slide 7: B4-10-5 CV
Chart: W14 - current on LGAD
| -2 | -27 | -52 | -77 | -102 | -127 | -152 | -177 | -202 | -227 | -252 | -277 | -302 | -327 | -352 | -377 | -402 | -427 | -452 | -477 | -502 | -527 | -552 | -577 | -602
Not annealed | -3.2e-07 | -1.157e-05 | -2.367e-05 | -2.855e-05 | -3.218e-05 | -3.573e-05 | -3.946e-05 | -4.35e-05 | -4.791e-05 | -5.281e-05 | -5.83e-05 | -6.456e-05 | -7.177e-05 | -8.019e-05 | -9.009e-05 | -0.000102 | -0.000116 | -0.000134 | -0.000155 | -0.000182 | -0.000217 | -0.000263 | -0.000325 | -0.000411 | -0.000538
10 min | 2.723e-06 | -3.0857e-06 | -1.7869e-05 | -2.3558e-05 | -2.6641e-05 | -2.9244e-05 | -3.1785e-05 | -3.4401e-05 | -3.7154e-05 | -4.0092e-05 | -4.3247e-05 | -4.6652e-05 | -5.0357e-05 | -5.4429e-05 | -5.8934e-05 | -6.3947e-05 | -6.9589e-05 | -7.596e-05 | -8.322e-05 | -9.1542e-05 | -0.000101 | -0.000112 | -0.000125 | -0.000141 | -0.000159 | -0.000182 | -0.000209 | -0.000244 | -0.000286 | -0.000339 | -0.000408
20 min | 2.763e-06 | -3.0813e-06 | -1.7483e-05 | -2.2991e-05 | -2.596e-05 | -2.845e-05 | -3.0889e-05 | -3.3405e-05 | -3.6049e-05 | -3.8878e-05 | -4.1913e-05 | -4.5199e-05 | -4.8776e-05 | -5.2718e-05 | -5.7081e-05 | -6.1937e-05 | -6.7402e-05 | -7.359e-05 | -8.0658e-05 | -8.8787e-05 | -9.8257e-05 | -0.000109 | -0.000122 | -0.000138 | -0.000157 | -0.00018 | -0.000209 | -0.000246 | -0.000294 | -0.000358 | -0.000447
40 min | 2.7607e-06 | -3.0818e-06 | -1.7125e-05 | -2.2393e-05 | -2.5234e-05 | -2.7597e-05 | -2.9925e-05 | -3.2319e-05 | -3.4821e-05 | -3.749e-05 | -4.0355e-05 | -4.3455e-05 | -4.6842e-05 | -5.0579e-05 | -5.4715e-05 | -5.9319e-05 | -6.4498e-05 | -7.0342e-05 | -7.6969e-05 | -8.4543e-05 | -9.332e-05 | -0.000104 | -0.000116 | -0.00013 | -0.000147 | -0.000167 | -0.000192 | -0.000225 | -0.000264 | -0.000316 | -0.000385
80 min | 1.8444e-06 | -3.5057e-06 | -1.676e-05 | -2.1786e-05 | -2.4484e-05 | -2.669e-05 | -2.8872e-05 | -3.1157e-05 | -3.355e-05 | -3.6108e-05 | -3.886e-05 | -4.184e-05 | -4.508e-05 | -4.8629e-05 | -5.2554e-05 | -5.6928e-05 | -6.1801e-05 | -6.7325e-05 | -7.3599e-05 | -8.0778e-05 | -8.914e-05 | -9.8787e-05 | -0.00011 | -0.000124 | -0.00014 | -0.00016 | -0.000184 | -0.000216 | -0.000257 | -0.000309 | -0.000386

## Slide 8: B4-13-5 CV
Chart: W14 - current on LGAD
| -2 | -26 | -50 | -74 | -98 | -122 | -146 | -170 | -194 | -218 | -242 | -266 | -290 | -314 | -338 | -362 | -386 | -410 | -434 | -458 | -482 | -506 | -530 | -554 | -578 | -602
Not annealed | 2.4868e-06 | -9.0838e-06 | -2.3174e-05 | -2.8504e-05 | -3.2582e-05 | -3.6592e-05 | -4.0908e-05 | -4.5666e-05 | -5.1005e-05 | -5.7083e-05 | -6.4096e-05 | -7.2329e-05 | -8.2126e-05 | -9.3903e-05 | -0.000108 | -0.000126 | -0.000149 | -0.000178 | -0.000217 | -0.000267 | -0.000335 | -0.000432 | -0.000578 | -0.000816 | -0.000815 | -0.000815
10 min | 2.916e-06 | -2.4152e-06 | -1.824e-05 | -2.4712e-05 | -2.8351e-05 | -3.1514e-05 | -3.466e-05 | -3.7991e-05 | -4.1582e-05 | -4.5503e-05 | -4.9817e-05 | -5.4604e-05 | -5.9961e-05 | -6.6048e-05 | -7.3003e-05 | -8.1028e-05 | -9.0408e-05 | -0.000101 | -0.000115 | -0.00013 | -0.000149 | -0.000172 | -0.000201 | -0.000238 | -0.000283 | -0.00034 | -0.000415 | -0.000513 | -0.000647 | -0.000827 | -0.000826
20 min | 2.9397e-06 | -2.3801e-06 | -1.7989e-05 | -2.4124e-05 | -2.759e-05 | -3.0625e-05 | -3.3656e-05 | -3.6856e-05 | -4.031e-05 | -4.4093e-05 | -4.8265e-05 | -5.2907e-05 | -5.8124e-05 | -6.4058e-05 | -7.0856e-05 | -7.8713e-05 | -8.7882e-05 | -9.88e-05 | -0.000112 | -0.000127 | -0.000146 | -0.00017 | -0.000199 | -0.000238 | -0.000287 | -0.000354 | -0.000444 | -0.000577 | -0.000798 | -0.000823 | -0.000823
40 min | 2.9404e-06 | -2.33e-06 | -1.7568e-05 | -2.3484e-05 | -2.6798e-05 | -2.9712e-05 | -3.2625e-05 | -3.5697e-05 | -3.9011e-05 | -4.2625e-05 | -4.6586e-05 | -5.0979e-05 | -5.5883e-05 | -6.1439e-05 | -6.7795e-05 | -7.5147e-05 | -8.3729e-05 | -9.3873e-05 | -0.000106 | -0.00012 | -0.000138 | -0.000159 | -0.000186 | -0.000221 | -0.000265 | -0.000322 | -0.000399 | -0.000506 | -0.000666 | -0.000824 | -0.000824
80 min | 2.3003e-06 | -2.4311e-06 | -1.6978e-05 | -2.2496e-05 | -2.5586e-05 | -2.8273e-05 | -3.0996e-05 | -3.3878e-05 | -3.6973e-05 | -4.0361e-05 | -4.4076e-05 | -4.8188e-05 | -5.279e-05 | -5.799e-05 | -6.3893e-05 | -7.0682e-05 | -7.8605e-05 | -8.7858e-05 | -9.8851e-05 | -0.000112 | -0.000128 | -0.000148 | -0.000172 | -0.000203 | -0.000243 | -0.000294 | -0.000364 | -0.000458 | -0.000604 | -0.000806 | -0.000806

## Slide 9: B4-16-5 CV
Chart: W14 - current on LGAD
| 0 | -20 | -40 | -60 | -80 | -100 | -120 | -140 | -160 | -180 | -200 | -220 | -240 | -260 | -280 | -300 | -320 | -340 | -360 | -380 | -400 | -420 | -440 | -460 | -480 | -500 | -520 | -540 | -560 | -580 | -600
Not annealed | 2.6907e-06 | -2.6523e-06 | -1.6761e-05 | -2.2542e-05 | -2.5648e-05 | -2.8349e-05 | -3.1085e-05 | -3.3954e-05 | -3.7033e-05 | -4.0384e-05 | -4.4053e-05 | -4.8107e-05 | -5.2628e-05 | -5.7731e-05 | -6.3533e-05 | -7.0186e-05 | -7.791e-05 | -8.695e-05 | -9.7614e-05 | -0.00011 | -0.000126 | -0.000144 | -0.000167 | -0.000195 | -0.000232 | -0.000277 | -0.000336 | -0.000414 | -0.00052 | -0.000669 | -0.00082
10 min | 2.7804e-06 | -2.4971e-06 | -1.6186e-05 | -2.1742e-05 | -2.4712e-05 | -2.7249e-05 | -2.9831e-05 | -3.2541e-05 | -3.5431e-05 | -3.8567e-05 | -4.1989e-05 | -4.577e-05 | -4.9969e-05 | -5.4686e-05 | -6.0013e-05 | -6.6076e-05 | -7.3058e-05 | -8.1153e-05 | -9.06e-05 | -0.000102 | -0.000115 | -0.000131 | -0.00015 | -0.000173 | -0.000202 | -0.000239 | -0.000283 | -0.000338 | -0.000406 | -0.000492 | -0.000614
20 min | 2.9397e-06 | -2.3801e-06 | -1.7989e-05 | -2.4124e-05 | -2.759e-05 | -3.0625e-05 | -3.3656e-05 | -3.6856e-05 | -4.031e-05 | -4.4093e-05 | -4.8265e-05 | -5.2907e-05 | -5.8124e-05 | -6.4058e-05 | -7.0856e-05 | -7.8713e-05 | -8.7882e-05 | -9.88e-05 | -0.000112 | -0.000127 | -0.000146 | -0.00017 | -0.000199 | -0.000238 | -0.000287 | -0.000354 | -0.000444 | -0.000577 | -0.000798 | -0.000823 | -0.000823
40 min | 2.7699e-06 | -2.4295e-06 | -1.5522e-05 | -2.0606e-05 | -2.3331e-05 | -2.5679e-05 | -2.806e-05 | -3.0588e-05 | -3.329e-05 | -3.6207e-05 | -3.9391e-05 | -4.2907e-05 | -4.6812e-05 | -5.1212e-05 | -5.6197e-05 | -6.1895e-05 | -6.8498e-05 | -7.6212e-05 | -8.5369e-05 | -9.6394e-05 | -0.00011 | -0.000129 | -0.000154 | -0.000191 | -0.000255 | -0.000363 | -0.000378 | -0.000379 | -0.000379 | -0.000379 | -0.000378
80 min | 2.6501e-06 | -2.3919e-06 | -1.4842e-05 | -1.9677e-05 | -2.2237e-05 | -2.4453e-05 | -2.6653e-05 | -2.8984e-05 | -3.1506e-05 | -3.4207e-05 | -3.7149e-05 | -4.0401e-05 | -4.401e-05 | -4.8076e-05 | -5.2667e-05 | -5.7911e-05 | -6.4006e-05 | -7.1146e-05 | -7.9602e-05 | -8.9779e-05 | -0.000103 | -0.000121 | -0.000147 | -0.000191 | -0.000264 | -0.000325 | -0.000333 | -0.000336 | -0.000332 | -0.00033 | -0.000331

## Slide 10: BACKUP – 80 °C

## Slide 11: Sr90 collected charge
T = –27 °C
Heavily annealed sample can be operated 200–300 V lower than standard annealed sample
  V6 fC = 220 V (prediction at 20 °C: 250 V), V6 fC = 420 V (prediction at 20 °C: 470 V)
    Excellent agreement, taking into accout T scaling (-1.1 V/K ?)
  V10 fC = 270 V, V10 fC = 520 V

## Slide 12: Leakage current
Leakage current measured during Sr90
  T uncertainty a few °C
    T is read out manually at the beginning of the measurement (highest voltage)
    Our logs say standard annealed was measured at –30 °C and heavily annealed at –27 °C
3x less current per fC in heavily annealed sample
per fC

## Slide 13: Time resolution
Time resolution consistent with charge collection results

## Slide 14: Dependence on time (space charge)
bulk layer dominated by deep defects (max. Ndeep~1014 cm-3)
gain layer dominated by initial acceptor term (NA~1016 cm-3)
initial acceptor removal c(NB,Feq,t)
deep defects behaviour with time
Hamburg model:
deactivation of effective acceptors
defects constant in time
activation of effective acceptors
The conclusion from the CV-IV measurements:
Vgl changes to less than 10% and remains almost constant after the initial period reached with standard annealing 80min@60C
Vfd changes as the annealing predicts for deep defects and reaches minimum in Vfd at around 80-300 min@60 C and then increases due to reverse annealing
At long and short annealing times LGADs perform better due to larger Vgl and at larger annealing times they perform better due to effects of the bulk on the electric field in the bulk.
G. Kramberger, HGTD week Feb 2026

## Slide 15: IT test structure and studied samples
  Irradiation Tests done on Quality Control Test Structure (QCTS) using 1 × 2 LGAD
    QCTS adjacent to each main sensor on wafer
    Channel size 2.1 mm × 0.8 mm (geometric capacitance same as pad on the main sensor)
    Same device measured with different methods to minimize systematics
    In production irradiate dies 10, 30 and 48 [•]
      Fluence 2.5e15 neq/cm2, annealing 80 min at 60 °C
  Electrical connections of 1 × 2 LGAD :
    CV/IV: one channel to Signal, one channel + guard ring to Guard
    Sr90: one channel to Signal, one channel + guard ring to Guard
    TCT: both channels to Signal, guard ring floating
LGAD1
LGAD2
Optical window in the interpad region
main 15 x 15 sensor
QCTS

## Slide 16: Correlation Vgl(TCT) vs. Sr90 charge (preproduction)
Correlation between Vgl from TCT and collected charge with 90Sr used to derive Acceptance Criteria
Cutoff Vgl corresponding to 5 fC (HGTD spec) is
  USTC-IME: 16.6 V
  IHEP-IME: 16.9 V
Cutoff Vgl (USTC-IME)
Cutoff Vgl (IHEP-IME)

## Slide 17: Correlation Gain(TCT) vs. Sr90 charge (IHEP-IME only)
Cutoff Gain(100 V) corresponding to 5 fC (HGTD spec) is 2.7 (IHEP-IME)
Not applicable for USTC-IME, since gain is smaller and uncertainty is large
Cutoff Gain
IHEP-IME only

## Slide 18: IT-QC: TCT results (preproduction)
Preproduction TCT results (Vgl and Gain (100 V)) as a function of fluence
  29 IHEP-IME wafers, 5 USTC-IME wafers
  Results slightly different between two designs (Gain (100 V)) not very sensitive on fluence in USTC-IME)
These results were correlated with 90Sr measurements to derive Acceptance Criteria