## Slide 1: Overview: Studied Targets & Challenges so far
Eleni Vagenaa, Fanouria Antonioub, Georgios Dianosa, Aristeidis Mamarasb, Vasilis Vlachoudisb, Ioannis Papaphilippoub, Charikleia Petridouac, Dimos Sampsonidisac
aAristotle University of Thessaloniki: University Campus, Thessaloniki, 54124, Greece;
bCERN, CH-1211 Geneva 23, Switzerland;
cCenter for Interdisciplinary Research and Innovation (CIRI-AUTH), Thessaloniki 57001, Greece;

## Slide 2: List of the radionuclides: that have been already studied and the ones that are currently under ongoing work
Radionuclide | Emission Type | Application | Beam Energy
COMPLETED STUDIES |  |  | 
177Lu | β⁻ emitter (+ γ) | Therapeutic | d, 17.9 MeV
161Tb | β⁻ emitter (+ Auger e⁻) | Therapeutic | d, 18 MeV (12-26 MeV)
155Tb | γ emitter | Theranostic / Diagnostic | d, 15 MeV (13-20 MeV) p, 10-20 MeV
152Tb | β⁺ / EC | Diagnostic / Dosimetry | d, 16 MeV (10-24 MeV) p,12 MeV (10-24 MeV)
ONGOING STUDIES |  |  | 
47Sc | β⁻ emitter (+ γ) | Therapeutic | 
44gSc | β⁺ emitter | Diagnostic | 
67Cu | β⁻ emitter (+ γ) | Therapeutic | 
64Cu | β⁺ / β⁻ / EC | Diagnostic / Theranostic | 

## Slide 3: Simulation Framework
Cross-section validation
Tool: Geant4 Monte Carlo (Agostinelli et al.)
Physics model: INCLXX
Simulation Code
1st step:
Thin target simulations compared against:
Experimental data from EXFOR database
Evaluated data: IAEA-therapeutic
Goal: how well does our model work for specific beams and energies?
Thick-Target Calculations
2nd step:
Simulate realistic targets under various irradiation conditions, regarding the irradiation time and beam current to estimate the yields.
Clinical Adequacy Assessment
3rd step:
Is what we produce useful for clinical use?
Comparison with standard protocols for therapeutic doses

## Slide 4: Results for 177Lu Production
Beam | Irrad. time | AEOB (GBq) | A48h (GBq)
1 mA | 5 days |  | 
1 mA | 12 days |  | 
2 mA | 5 days |  | 
2 mA | 12 days |  | 
5 mA | 5 days |  | 
5 mA | 12 days |  | 
Beam | Irrad. time | AEOB (GBq) | A48h (GBq)
1 mA | 5 days |  | 
1 mA | 12 days |  | 
2 mA | 5 days |  | 
2 mA | 12 days |  | 
5 mA | 5 days |  | 
5 mA | 12 days |  | 
1 mA / 5 days → ~44 cycles | ~11 patients/run
2 mA / 12 days → ~155 cycles | ~38 patients/run
10 mA / 12 days → ~777 cycles | ~194 patients/run
Clinical Adequacy
(Standard protocol: 9 GBq/cycle, 4 cycles/patient)
Graph: How the activity evolves during a 5-day irradiation scenario and during 48 h cooling
Lu-177
growing even after the beam stops
(177Yb decay)
Short-lived: decay quickly
Main impurity: 175Yb
Activity at EOB & after 48h cooling (GBq) — beam current scaling
Target: 97% enriched 177Yb₂O₃ | production routes: (d,n)

## Slide 5
Clinical Adequacy (9 GBq/cycle, 4 cycles/patient)
Beam | Irrad. time | AEOB (TBq) | A48h (TBq)
1 mA | 5 days |  | 
1 mA | 10 days |  | 
2 mA | 5 days |  | 
2 mA | 10 days |  | 
Beam | Irrad. time | AEOB (TBq) | A48h (TBq)
1 mA | 5 days |  | 
1 mA | 10 days |  | 
2 mA | 5 days |  | 
2 mA | 10 days |  | 
Activity at EOB & after 48h cooling (GBq) — beam current scaling
1 mA / 5 days → ~113 cycles | ~28 patients
1 mA / 10 days → ~181 cycles | ~46 patients
2 mA / 5 days → ~226 cycles | ~57 patients
2 mA / 10 days → ~363 cycles | ~90 patients
At 1mA we get TBq that supports ~28 patients
Target: 95% enriched 160Gd₂O₃ | production routes: (d,n)
Results for 161Tb Production
The plot shows the activity evolution of 161Tb and its main contaminant 160Tb during and after a 5-day irradiation at 18 MeV
Need for Tb-161 / Tb-160 separation
The main concern with Tb-161 production is Tb-160 — due to its long half-life of 72 days

## Slide 6: Results for 152Tb Production
After 48 h of cooling, short-lived 152Tb significantly decrease, while longer-lived isotopes remain relatively stable
Target: 30% enriched 160Gd₂O₃ | 2 production routes: (d,n) & (d,p)
Comparison of yields – purity: deuteron vs proton beams
Both deuteron and proton beams yield comparable Tb-152 activities (~40–55 MBq/μA/h) and purity (~65–70%) in their optimal energy windows (deuterons at around 18 MeV & protons at around 15 MeV)
Tb-152 can be produced equally, regardless of the available beam type (advantage).

## Slide 7
Beam | Irrad. time | A_EOB (TBq) | A_48h (TBq)
1 mA | 5 days |  | 
1 mA | 10 days |  | 
2 mA | 5 days |  | 
2 mA | 10 days |  | 
Beam | Irrad. time | A_EOB (TBq) | A_48h (TBq)
1 mA | 5 days |  | 
1 mA | 10 days |  | 
2 mA | 5 days |  | 
2 mA | 10 days |  | 
Target: 93% enriched 155Gd₂O₃ | 2 production routes: (d,n) & (d,p)
Results for 155Tb Production
250 GBq@1mA,5d
1 TBq@1mA,5d
Deuterons: purity ~75–80% at 13–16 MeV with increasing yield (a good production window).
Protons: purity collapses already at 13 MeV. Above 14 MeV, production of Tb-154 dominates due to the opening of the (p,2n) channel.
Deuterons offer better combination of yield and purity.

## Slide 8: Main challenge: Target’s (176Yb2O3 ) Thermal Stress due to High-Currents
Material properties of 176Yb2O3
Thermal conductivity k: 4–9 W m⁻¹ K⁻¹
Thermal exp. coeff. (TEC): (8.5 ± 0.6) × 10⁻⁶ K⁻¹
Young's modulus E: 130–170 GPa
Poisson's ratio ν: ≈ 0.30
Fracture strength: 100–200 MPa
BEAM CONDITIONS
Projectile: Deuterons, 17.9 MeV
Beam current: 1 mA → up to 5 mA
Beam area: 3.14 cm² (r = 1 cm)
Energy deposited ΔE: ≈ 9.9 MeV (17.9 – 8 MeV exit)
Target thickness: 0.36 mm ¹⁷⁶Yb₂O₃
Quantity | Value
Deposited power | ~9.9 kW
Heat flux | ~3.15 kW/cm²
Temperature rise (ΔT) | ~800 K
Thermal stress | ~1.7 GPa
We ESTIMATED THERMAL IMPACT @ 1 mA
Thermal stress is 10 times the fracture strength of material (100–200 MPa fracture strength)
proper cooling is essential

## Slide 9: Addressing Thermal Challenges: Solutions & Ongoing Collaboration
Group: Praena et al., University of Granada
Recent Publication: Proposed a Cooling system design for 177Lu production using Copper backing with milichannel water cooling @ IFMIF-DONES
López-Melero et al. (2021)
Recently started Collaboration
Goal: simulate a proper target-backing system model.
ANSYS software for Thermal-Mechanical Analysis (Ongoing)
Backing material is crucial: We’ll start study materials such as Ta, Al, Ti and SS316
Possible good candidates: Tantalum, Titanium: which based on their TEC parameters are much closer to Yb₂O₃ and this may lead to more mechanically robust target-backing system.
Candidate Backing Materials Under Study

## Slide 10: Summary
COMPLETED
177Lu — d, 17.9 MeV | ¹⁷⁶Yb₂O₃
~11 patients/run @ 1mA /5 days
161Tb — d, 18 MeV | ¹⁶⁰Gd₂O₃
~28 patients @ 1 mA / 5 days
155Tb — d/p, 15 MeV | ¹⁶⁰Gd₂O₃
>1 TBq @ 1 mA / 5 days
152Tb — d 16 MeV / p 12 MeV
Yield vs purity studied
Ongoing Work
47Sc, 44Sc, 67Cu, 64Cu production studies in progress
ANSYS thermal-mechanical simulations for target design
Optimal backing material selection (Cu, Ta, Ti..) under study
Thank you
Key Findings
Geant4-based simulation:
successfully reproduce experimental cross-sections
enables reliable thick-target yield predictions across the studied radionuclides.
Activities achieved are clinically adequate
Proper cooling must be designed to minimize the target’s thermal stress