## Slide 1: DRD3: Overview of activities linked to JSI/F9 G. Kramberger for the colleagues involved in the DRD3 activities Bojan Hiti, Alissa Howard, I. Mandić, Marko Puklavec, Ajda Osterman, Iskra Velkovska, Marko Zavrtanik
DRDs started with the “bible” document for detector RD in the next decades – F9 took a visible role in shaping of that document (for Solid State Detectors - DRD3 and Photon detection – DRD4)
a special mention goes to our BSc. and MSc. students:
Bor Kokovnik
Urban Mernik
Matic Terglav

## Slide 2: DRD3 Collaboration
124 institutions (+17 observers) / 700++ people in the community e-group
Status of Collaboration – timeline of past years:
12-2023 - provisional approval
01-2024 - formation of CB
03-2024 - election of SP
05-2024 - formation of WG-WPs
06-2024 - approval (scientific proposal)
06-2024 - first DRD3 week
07-2024 - start of scientific meetings
and preparation of
WP projects
10-2024 - approval of the DRD3 rules
12-2024 - second DRD3 week
01-2025 - finalization of WP projects
(adjustment to funding reality)
02-2025 - first DRDC review
06-2025 - third DRD3 week
approval of the first WP projects
10-2025 – Jamboree week
11-2025 - fourth DRD3 week
12-2025 - draft of MoU Annex sent to CERN
2-2026 - second DRDC review
5-2026 - rules on the formation of RB
6-2026 - fifth DRD3 week
Large interest from the community:
collaboration regularly receives requests for joining it
Large presence at DRD3 weeks (~250 people, ~80 contributions)

## Slide 3: Our mission and organization
Working group (WG) - long term collaborative R&D activity linked to certain technology/purpose/application/method aiming to fulfil the research goals. This encompasses R&D that can be also outside DRDTs, but is related to semiconductor detectors, e.g.:
    R&D outside particle physics application with benefits for HEP
    novel semiconductor material characterization ideas
    technologies not yet listed in the DRDTs
Working package (WP) - short/midterm strategic R&D activity reflected in the ECFA detector roadmap document – DRD Themes. The research should not be related to a specific approved experiment.
Common Collaboration Fund – finance Blue-sky R&D, small projects, common hardware, common activities (e.g. organization of the schools, thesis awards, test-beam/laser-test/irradiation campaigns) – not meant for funding the labour.
WG1 – monolith
WG2 – hybrid
WG3 – silicon at extreme fluences
WG4 – simulations
WG5 – facilities and techniques
WG6 – WBS
WG7 – interconnections
WG8 – outreach

## Slide 4: DRD3 – structure of the collaboration
WG conveners serve also as WP conveners
Each work package consist of several WP projects – all not yet fully resource loaded
Each work package project should address the themes from the road map document (one-to-one)
September 2026
Resource Board is in formation.
We have also a role or Resource Coordinator to communicate with FA

## Slide 5: Paths of present silicon sensor R&D
Hybrid devices
(WG2/WP2-4D tracking)
with Gain
with Gain
(LGAD)
column 3D
trench
3D
Monolithic devices
( WG1/WP1-CMOS )
55-180 nm processes
large area passive devices
(strips)
with gain
DepletedMAPS
w/o gain
depleted MAPS
w/o gain
with gain
MAPS
optimized for hit rates, radiation hardness and temporal resolution
optimized for power, material and position resolution
proven/demonstrated
recent research (working prototype)
proof of concept ongoing
Small electrode devices
Large electrode device
3D devices
Planar
F9 - involvement

## Slide 6: WG1/WP1 Monolithic silicon sensors
MAPS for FCC-ee
Vertexing application:
  very high spatial resolution (≤3 µm) - pixels 15-25 mm2
  high data rate (~100 MHz/cm2)
  radiation tolerance (>1013 neq/y cm2 NIEL , and <1 Mrad/y)
  low mass (0.05% X0 inner layers ITS3 like, to 0.2-0.3% X0 staves at outer layers)
  good timing/time stamping (~20 ns – power consumption driven)
  small power (<40 mW/cm2)
Tracking application:
  high spatial resolution (~5-7 µm in r-phi) - elongated pixels
  data rate (~100 kHz/cm2)
  radiation tolerance – negligible (>1010 neq/y cm2 NIEL , and <4 krad/y)
  Material budget (~1% X0)
  good timing/time stamping (>100 ns)
  small power (~<150 mW/cm2)
Calorimetry
  are present standard planar technologies good enough?
Constraints:
  process : CiS or HVCMOS inherently linked to small and large electrode designs
  enough epi-thickness (CiS) and application of hi-res wafers (HVCMOS)?
  stitching option for vertex detectors
  enough wells and metal layers for complex processing
taken from N. Wermes
LARGE ELECTRODE DESIGN
SMALL ELECTRODE DESIGN
TWO approaches
This is likely the long term direction that we need to start preparing for!
(on the sensing part and testing we are well set – Marko moves to ASICs readout)

## Slide 7: WG2/WP2: Hybrid silicon technologies and 4D tracking - LGAD
Limitations for conventional LGADs:
Fill factor (large cell devices) due to JTE
Radiation harness – currently to ~3e15 cm-2
Typically 20-55 mm thick with signals of 20fC (G~40)
LGAD are planar technology that can provide superb temporal and position resolution.
Future R&D is all about the precision in 4D (~10 mm, <30 ps):
small pitch or resistive sharing for lower hit rates environments
timing resolution with small power consumption. In planar technology fast/thin detectors with gain to reduce electronics jitter, landau fluctuations and ToA contribution (weighting field)
We were among proposers of the LGADs
Examples

## Slide 8: WG2/WP2: 4D tracking – LGADs (FCC-ee, HL-LHC Run5 upgrades, EiC, …)
Radiation hardness (highly active field of research) is almost 2 orders of magnitude lower for FCC-ee applications. No special treatment of gain layers (carbon enrichment) is needed.
Fill factor
  relatively low rates at larger radii allow for Resistive Silicon Detector approach
  (AC-LGAD, DC-LGAD)
  possible use of iLGAD – collection of holes is not a problem
  TI-LGAD designs (high rate & small pitch devices)
Novel algorithms to exploit ML/AI to reconstruct position/hit time
Production of LGADs has been transferred to CMOS foundries – integration of electronics may be feasible
4D tracking may be sacrificed for lower power consumption
A small pitch LGAD with close to 100% fill factor for high rate environments.
FBK TI-LGADs
(AIDAINNOVA design)
RSD – FBK
Test Beam
RSD – FBK
Test Beam
4% of the pitch
INFN -TO
Our group involved in two WP2 projects on LGADs (Marko/Ajda –AC-LGAD and Iskra TI-LGAD)

## Slide 9: WG2/WP2: 3D sensor technologies with gain (LHCB-Velo upgrade, FCC-hh, …)
2018-RD50 workshop

## Slide 10: 3D sensors with gain – new advances
During the ECFA detector roadmap document preparation:
“Improvements of aspect ratio to 100:1 would lead to manufacturing of very narrow columns <1 mm with thicknesses of ~100 mm which could lead to electric fields high enough (~30 V/mm) for multiplication”
IME 8” CMOS process
30-35 mm thick epi on thick substrate
n+ columns on p type bulk
Neff=2∙1013 cm-3
ASPECT RATIO OF 100:1
DRD3 WP2 project “Novel silicon 3D-trench pixel detectors based on 8-inch CMOS process”
(Marko and Ajda are involved)

## Slide 11: 3D sensors with gain – F9/TPA
depletion
fully depleted wo gain
gain region
z=17 mm
JSI TPA setup
(Marko Z. & Bojan’s development)
accepted to IEEE TNS

## Slide 12: WG3&WG6 – defects and extreme fluences
Our group is very active in radiation damage studies and extreme fluences
  impact ionization and mobility measurements up to FCC-hh levels (Ajda’s thesis, Marko’s thesis)
  initial dopant removal – mainly acceptors (Alissa’s – just defended and Iskra’s thesis)
    long term and high temperature annealing studies (Ajda’s thesis)
    compensated LGADs – parametrization
    partially activated boron (Iskra’s thesis)
We are active in WBS semiconductors (GaN/SiC projects) – mainly for irradiations and materials (Igor)
C B
B deactivated
B still activate
Alissa's thesis

## Slide 13: WG4 – simulations
“Monte Carlo”
(predicting the performance of complex detector assemblies)
TCAD
(understanding the sensors)
GOALS:
Developing and verification of damage models (effective and defect based)
Establish how to benchmark/evaluate the models against the measured properties (important milestone)
Improving the TCAD with new findings (WBS, extreme fluences)
Develop a flexible framework to simulate performance of different processes (CMOS)
GOALS:
Implementation of improved semiconductor models (e.g. mobility, impact ionization, trapping …)
Adaptation of WBS sensors
Adaptation of dynamic /adaptive E,Ew
Implementation of common electronics/digitization
GEANT4
E,Ew
AllPix2 / Garfield++ as the main tool
complement by other ones (KDetSim, WF2)
Synopsis, Silvaco …
At some point we will have to touch TCAD
Plans to have software suits as ISF-I center
KDetSim used in most of our simulations!

## Slide 14: WG5 – techniques and facilities
Irradiation facility – still and will remain to be the reference in HEP (Igor is the main force behind e.g. organization of extreme fluence campaigns 1e18 cm-2)
Example: development of new techniques for AC-LGADs where double-pulse/rate capabilities can be fully tested DB-TCT (double beam TCT) – positioning beams to micron precision with tuneable delays
New scanning 90Sr timing setup (Marko P.’s thesis in the scope of DRD3/HGTD developments)

## Slide 15: WG8 – Outreach
2nd TCT school
CERN
1st TCT school at CERN
Organization of the DRD3 TCT schools (schools are heavily oversubscribed)
Bojan is the key person – already 3rd edition)
Particulars (JSI-F9 spin out company) provides two measurement setups

## Slide 16: Conclusions
DRDs are general R&D frameworks therefore it is our mission to bring the technological readiness of a certain technology to the point where approved experiments can take it and tailor it to the specifics of the project.
F9 is a very visible member of the collaboration with currently 3 theses in preparations (Iskra, Marko and Ajda):
  We take part in total of 3 WP2 projects (AC-LGADs, TI-LGADs, 3D with gain)
  We take part in 1 WP3 project (radiation damage of LGADs)
  We take part in 2 WP3/WG6 projects (GaN and SiC – mainly irradiations)
  We are very active in WG5 convened by Bojan (TBs, new setups)
  We take part in WG8 program (TCT school)
Very near future R&D (HGTD replacements)
  TI-LGADs (improvement of fill factor)
Near future oriented R&D (FCC-ee):
  Our involvement in MAPS is the next important decision (hardware infrastructure is being built, TCAD tools, …) in the first stage mainly in testing and concentrating to sensor-element. FCC-ee is the main driver for Vertex and Tracker detectors with MAPS
  AC-LGADs is the hybrid choice for ToF tracker/wrapper for some detector concepts (e.g. IDEA)
Long term and blue sky R&D (FCC-hh, ….)
  3D with gain
  Extreme Radiation Hardness – Wide-Band-Gap semiconductors
Developments outside HEP – military, medical, fusion